SECTION 203

EXCAVATION AND EMBANKMENT

Sect 203: CR2034.3.2.1.E92

Related Sect/Sp:  703/CR7031.E95

E92 – adding glass to embankments.

E65 include in FED and SOA funded projects.

CR3032 – ditch linear grading.  CR203.3 – compaction near large structure foundations. CR2031 – piezometers and settlements platforms.

E65 include in FED and SOA funded projects.

Special Provisions

203-1.01 DESCRIPTION.  Add the following:

Ditch linear grading shall consist of the final shaping of designated ditches and slopes for drainage by grading with a small dozer, motor grader, or other suitable means approved by the Engineer.

CR2032-010114

Add the following:

This work also includes fabrication, installation, maintenance, and removal of piezometers and settlement platforms as shown in the plans and directed by the Engineer.  The Department will monitor and record the data from the settlement platforms and piezometers.

CR2031-010610

Standard Modification

203-2.01 MATERIALS.  Add to the end of this subsection.

6.	Crushed Glass:  May be combined with soil-aggregate material to be used in embankment construction.  Meet 703-2.15 requirements.

203-3.01 GENERAL.  Add to the end of this subsection.

Do not place soil-aggregate containing glass cullet:

1.	Within four feet from the face of any embankment slope,

2.	Within 150 feet from any surface water body,

3.	In embankment areas where culvert placement is required,

4.	In contact with any geosynthetic material.

E92-080112

Add No. 5:

5.	Within 50 feet of detection loops.

CR203.4-022015

203-3.03 EMBANKMENT CONSTRUCTION.  Add the following after the last paragraph:

Furnish the materials, fabricate, install, and maintain the settlement platforms and piezometers as shown in the plans and as directed by the Engineer.  Remove the settlement platforms, and piezometers, and grout solid the remaining pipe and conduit as shown in the plans when directed by the Engineer.

CR2031-010610

203-3.04 COMPACTION WITH MOISTURE AND DENSITY CONTROL.  Add the following:

Compact the embankment within 20 feet of a bridge abutment full width to not less than 100 percent of the maximum density.  Material used within this zone shall be graded to pass the 3 inch sieve.

CR203.3-110502

203-4.01 METHOD OF MEASUREMENT.  Add the following:

9.	Item 203(27).  Measurement of ditch linear grading, whether flat bottom or “V” ditch, will be measured for payment by the station along the center of the ditch for each ditch so designated, constructed, and accepted by the Engineer.

203-5.01 BASIS OF PAYMENT.  Add the following:

Payment for ditch linear grading will be full compensation for furnishing equipment, labor, tools, and incidentals to provide the preparation, excavation and shaping necessary to complete the work.

Payment will be made under:

Pay Item No.	Pay Item	Pay Unit

203(27)	Ditch Linear Grading	Station

CR2032-010114

Add the following:

Grading and placement of material used within 20 feet of bridge abutments will not be paid for directly but will be subsidiary to Pay Item 203(6A) Borrow, Type A.

CR203.3-110502

Add the following:

The Contract unit price includes furnishing the materials, fabricating, installing, maintenance, removal of settlement platforms and piezometers, removal of conduit and steel pipe and grouting the remaining conduit and steel pipe solid.

Payment will be made under:

Pay Item No.	Pay Item	Pay Unit

203(19A)	Settlement Platforms	Each

203(19B)	Piezometers	Each

CR2031-010610