SECTION 203

EXCAVATION AND EMBANKMENT

Sect 203: CR2032.1.CR113.E92

Related Sect/Sp:  703/CR7031.E95

E92.  Crushed glass added to embankment.

E65 include in FED and SOA funded projects.

Standard Modification

203-2.01 MATERIALS.  Add to the end of this subsection.

6.	Crushed Glass:  May be combined with soil-aggregate material to be used in embankment construction.  Meet 703-2.15 requirements.

203-3.01 GENERAL.  Add to the end of this subsection.

Do not place soil-aggregate containing glass cullet:

1.	Within four feet from the face of any embankment slope,

2.	Within 150 feet from any surface water body,

3.	In embankment areas where culvert placement is required,

4.	In contact with any geosynthetic material.

E92-080112