SECTION 505

PILING

Sect 505: CR5051.65

Related Sect/Sp:  504/CR224.E39, 660/CR6601, 668/CR668

Use with all High Tower lighting.

Special Provisions

505-3.07 EXTENSIONS, SPLICES, AND BUILD-UPS.  Add the following after the 2nd paragraph in No. 1:

High Tower Piling.  Field splices shall be located a minimum of 10 ft from either end of the pile and limited to one per 40 ft of pile length.  Make splice with complete-joint-penetration groove weld with backing ring.

Replace the last paragraph with the following:

Meet the welding requirements of Subsection 504-3.01.8 and the following:

High Tower Piling.

1.	Joint Preparation.

Cut off pile perpendicular to pile centerline, "freehand" cutting is prohibited.  Before welding, prepare pile top establishing the proper groove angle with a pipe beveller.  Touch up and repair surfaces to be welded by grinding.  Clean pile ends inside and out for a width of 4 inches perpendicular to the groove, for the length of the groove, each side of the groove removing all moisture, grease, rust, mill scale and other that might negatively influence the weld quality.

2.	Weld Inspection.

a.	Visual Inspection (VT)		100%

b.	Ultrasonic Testing (UT)		100%

Inspection and testing by a third party American Welding Society (AWS) Certified Weld Inspector (CWI) qualified to perform Nondestructive Examination (NDE) of welds.

505-5.01 BASIS OF PAYMENT.  Add the following to the second paragraph:

Include costs for furnishing and installing piles for High Tower Lighting in Pay Item 668(1) High Tower Lighting System Complete.

CR5051-012710