SECTION 508

WATERPROOFING MEMBRANE

Sect 508: CR5081.E36

Related Sect/Sp:  202/CR2023, 641/CR641, 643/CR6431

Do not use the Bridge Department's Section 508 provisions – not included here, without Proj Managers & Construction Engineers approval.

Special Provisions

508-1.01 DESCRIPTION.  Add the following:

Comply with the Construction General Permit, issued by the ADEC under the NPDES and Section 641 during all phases of construction including the removal of existing asphalt pavement, the waterproofing membrane, and the application of a new membrane, asphalt, and concrete materials.

Remove the existing asphalt pavement and membrane waterproofing on the following bridges:

| Bridge Number | Bridge Name |
| --- | --- |

CR5081-100312

Standard Modifications

508-2.01 MATERIALS.  In paragraph titled Membrane Material, remove the text:  "Approved Products List" and replace with:  Qualified Products List

E36-012707

508-3.01 APPLICATION OF MEMBRANE WATERPROOFING.

1.	General.  Replace a. b. c with the following and add d.

a.	Complete bond between the leveling course and concrete bridge deck.

b.	Complete bond between the membrane and the leveling course.

c.	Unbroken waterproof membrane in place between the leveling course and the asphalt overlay.

d.	Complete bond between the membrane and the asphalt overlay.

2.	Preparation of Concrete Deck.  Before applying membrane:  Replace a. through f. with the following:

a.	Remove existing asphalt, concrete, and membrane down to the base concrete bridge deck.

b.	Do not employ removal methods, manual or mechanical, that damage the concrete deck.  Mechanical milling machines such as a reclaimer or planer must not damage the concrete deck.

c.	Remove any contaminants such as grease, oil or paint with solvents, detergents or by sand blasting as approved by the Engineer.  Do not damage the existing concrete deck and deck materials.

d.	Sweep the deck to remove all foreign materials such as dirt, dust, moisture, and loose concrete.  Sweep and or power broom per Subsection 643-3.04 Traffic Control Devices, Item 6., Street Sweeping and Power Brooming.

e.	Before applying the tack coat, primer, or emulsion, thoroughly clean the deck with compressed air.  Disturbed particles, dust or other shall be contained similar to the requirements for street sweeping and power brooming.

f.	Prevent foreign material from entering streams including fugitive dust particles.

508-5.01 BASIS OF PAYMENT.  Replace the second paragraph with the following:

Leveling course and asphalt overlay are paid for under the paving items.

Pavement planing on bridge decks is paid for under 202(15) Pavement Planing.  Additional removal of existing pavement below the pavement planing depth to bare concrete deck is subsidiary to 508 pay items.  Removal of existing waterproof membrane is subsidiary to 508 Pay Items.

Payment will be made under:

Pay Item No. 	Pay Item	Pay Unit

508(1_)	Waterproofing Membrane Bridge No.         	Lump Sum

CR5081-100312

1ST bridge pay item would be 508(1A), 2nd 508(1B), etc.  Fill in the bridge number relative to each pay item.