Special Provisions

Sect 514: CR514

Related Sect/Sp:  608/CR6082.1

Add the following Section:

SECTION 514

CONCRETE SURFACE TREATMENTS

514-1.01 DESCRIPTION.  This work consists of providing an aesthetic fascia on precast and cast-in-place concrete walls.  Use form liners on all cast-in-place concrete retaining walls.  Install anti-graffiti protection on the walls and surfaces designated in the Plans.

514-2.01 MATERIALS.  Reinforcing steel shall meet the requirements of Subsection 709-2.01 Reinforcing Steel.

Designer, provide two examples of each pattern specified.

Provide standard reusable, nonporous form liners conforming to the pattern for Burke Form Liner No. BG 312, Waterfall; provide another pattern, or approved equal.

Use a two step graffiti protection system designed specifically for this use.  The system shall consist of a single component clear acrylic base coat covered by a clear urethane finish coat.  This material is not a sealer, or vapor barrier.  No appreciable discoloration is allowed.  The Engineer will determine the level of discoloration permitted.

Trained personnel shall apply the material according to the manufacturer's recommendations.

514-3.01 AESTHETIC FASCIA.  Use form liners with the retaining wall forms where the vertical concrete surface will be exposed.  The wall dimensions and concrete quantities provided on the Plans are minimums and do not include allowances for the thickness of the form liners.  The Contractor shall account for the concrete quantity and dimensions associated with the form liner.

The liners will cover the majority of the concrete vertical surface.  Install the liners with a minimum of 2 inches and a maximum of 12 inches between the edge of the liner and the finished top of wall, the pathway surface, or the original ground grade at the bottom, and edge or expansion joints on all sides of the wall.  The Engineer must review the placement of the liner on the form surface and either approve the placement and installation or provide directions for changes, corrections, or adjustments required.  Written approval of the form liner placement and installation, from the Engineer, is required before concrete may be placed.

514-3.02 ANTI-GRAFFITI PROTECTION.  Allow 28 days after the forms are removed from the concrete surfaces before applying coatings.  Apply base coat with a roller or sprayer in accordance with the manufacturer's recommendations.  Apply two finish coats after the base coat has cured for 72 hours.  Apply masking as required.

514-4.01 METHOD OF MEASUREMENT.  Section 109 and the following:

Aesthetic Fascia:  Measure aesthetic fascia by the square foot of actual design exposed in the finished structure regardless of type.

Anti-Graffiti Protection:  Measure anti-graffiti protection by the square foot of surface area designated by the Engineer.

514-5.01 BASIS OF PAYMENT.  Payment for concrete surface treatments will be full compensation for labor, equipment, and furnishing materials including reinforcing steel, required to complete the walls in accordance with the Plans and Specifications.

Payment will be made under:

Pay Item No.	Pay Item	Pay Unit

514(1)	Aesthetic Fascia	Square Foot

514(2)	Anti-Graffiti Protection	Square Foot

CR514-072011

Designer, confirm the reinforcing, concrete, forming, concrete placement, curing and finishing is covered here or elsewhere.