SECTION 703

AGGREGATES

Sect 703: CR7031.E95

Related Sect/Sp:  301/CR176.26; 203/E92, 301/E93; 304/E94

Related Sect/Sp:

E95 – crushed glass material.

Standard Modification

Add new subsection 703-2.15.

703-2.15 CRUSHED GLASS.  Up to 10% by weight crushed glass (cullet) smaller than 3/8-inch may be uniformly blended with natural soil-aggregate material prior to project delivery and placement.  Glass cullet must be free of soil, paper, plastic, metals, organic material and other deleterious and hazardous substances.  No more than 2.0% debris should be present as determined by Section X3 of AASHTO M318.

Eligible glass products from which glass cullet might be produced include: food and beverage container glass; plain ceramic or china dinnerware; or building window glass.

Prohibited glass products include: automobile windshields or other glass from automobiles; light bulbs of any type; porcelain products; laboratory glass; television, computer or other cathode ray monitor tubes.

Provide documentation certifying that the glass cullet:

1.	Showing the origin of the glass products,

2.	Does not contain prohibited materials,

3.	Meets debris content requirement.

Uniformly blend glass cullet and natural soil-aggregate and meet the following gradation requirements for the type specified:

TABLE 703-13

| Type (Section) | Section/Table |
| --- | --- |
| Selected material (203-3.03) | Section 703-2.07 |
| Base Course (301) | Table 703-2 |
| Subbase (304) | Table 703-8 |

For the natural soil-aggregate used in the blend, meet quality requirements as shown in Table 703-1, Section 703-2.07, or Section 703-2.09 for the type specified.

E95-080112