SECTION 712

MISCELLANEOUS

Sect 712: CR246.E99.46

Related Sect/Sp:  604/CR6041, 627/CR6271; 643/CR6437, 670/CR246

Related Sect/Sp:

Standard Modifications

Replace Subsection 712-2.08 with the following:

712-2.08 GLASS BEADS.  Submit certifications of compliance as specified in Section 106-1.05 for each lot of glass beads used on the contract.  Glass beads shall contain no more than 200 ppm of lead, 200 ppm of antimony, or 200 ppm of arsenic when tested in accordance with EPA 40 CFR 261.4.  Glass beads shall meet AASHTO M 247, Type 1, with a moisture resistant coating when tested in accordance with AASHTO TP 97.

E99. Standard Modification is for glass beads in paint, not MMA. Exclude if marking material is MMA and not paint.

E99-051513