SECTION 202
REMOVAL OF STRUCTURES AND OBSTRUCTIONS

Sect 202: SSP34

Related Sect/Sp:  CR202.1.2.3.4.5.6.SSP31

Special Provisions

Replace Subsection 2.01 with the following:

202-2.01 MATERIALS. Use materials that conform to the following:

Timber	AASHTO M 168 (Hemlock, Douglas fir, Western Pine, or Sitka Spruce). Pressure treated per AASHTO M 133.

Steel Pipe	Standard Weight Steel Pipe, 2-inch (max.) diameter. Galvanized per AASHTO M 111.

Steel Fasteners	ASTM A307, Grade A. Galvanized per AASHTO M 232.

Reflectors	Yellow acrylic prismatic type meeting AASHTO M 290 or retroreflective sheeting meeting ASTM D4956, Type III, IV, or V.

SSP34-010116