Special Provision

Sect 507: Specials SSP18. Coordinate with Bridge Dept. project specials. SSP18 will be further reviewed when SSHC 2016 is issued.

Related Sect/Sp:

2016 SSHC replacement Section 507 specification for 2015 SSHC Section 507. May be removed after the issue of the 2016 SSHC.

- Replace Section 507 with the following:

- SECTION 507

BRIDGE BARRIERS AND RAILING

507-1.01 DESCRIPTION. Construct concrete, timber, or steel bridge railing, pedestrian railing and safety railing as shown on the Plans. Furnish and install bridge number plates as shown on the Plans.

507-2.01 MATERIALS. Use materials that conform to the following:

Steel Railing	Section 722

Timber Railing	Section 506

Concrete	Section 501

Epoxy-Coated Reinforcing Bars	Subsection 709-2.01

Grout	Section 701

Cable	Use ¼ inch galvanized wire rope with a minimum breaking force of 7,000 pounds.

Bronze	ASTM B98, UNS Alloys C65100 or C65500 or

ASTM B584, UNS Alloy C92200

CONSTRUCTION REQUIREMENTS

507-3.01 CONSTRUCTION REQUIREMENTS.

1.	General. Construct railing to the line and grade shown on the Plans. Ensure that the rail does not reflect any unevenness of the bridge structure. Set rail posts plumb. Place railing after all falsework is removed and the span is self-supporting. Do not paint bridge railing.

Furnish and install concrete curbing, associated reinforcing steel, and the approach rail transition bracket for steel bridge railing.

2.	Steel. Erect steel railing in conformance with Section 504, except do not use load indicating washers. Weld in conformance with Section 504. Complete welding before galvanizing the railing.

3.	Timber. Fabricate and install timber railing according to Section 506.

4.	Concrete. Construct concrete barriers to meet applicable requirements of Sections 501 and 503. Use Class A concrete with a specified compressive strength of 4000 psi. Apply a rubbed finish to exposed surfaces of concrete.

507-4.01 METHOD OF MEASUREMENT. Section 109.

507-5.01 BASIS OF PAYMENT. The contract price includes all rail elements, rail posts, brackets, spacers, fastenings and anchors required to attach the railing to the structure; concrete and associated reinforcing steel included or partially contained within the limits of the concrete rail section or within the limits of the concrete curb for the steel bridge rail section; and bridge number plates.

Payment will be made under:

Pay Item No.	Pay Item	Pay Unit

507(1)	Steel Bridge Railing	Linear Foot

507(2)	Pedestrian Railing	Linear Foot

507(3)	Thrie Beam Bridge Railing	Linear Foot

507(4)	Concrete Barrier	Linear Foot

507(5)	Timber Bridge Railing	Linear Foot

507(6)	Cable Safety Railing	Linear Foot

SSP18-010116