SECTION 702
ASPHALT MATERIALS

Sect 702: CR702.2

Related Sect/Sp:  306/CR306, 401/CR401, 408/CR408

Special Provision

CR702.2. Include all projects with asphalt.

702-2.03 EMULSIFIED ASPHALT.

2.	Special Tack Emulsion, STE-1.

TESTS ON RESIDUE

Replace the first line: 	Penetration @ 77 °F	100-200,

with:	Penetration @ 77 °F	100-250

CR702.2R1-060115