SECTION 705
JOINT MATERIALS

Sect 705: Section Specials SSP25. SSP25 will be further reviewed when SSHC 2016 is issued.

Related Sect/Sp:  501

Special Provisions

Delete Subsections 705-2.02 Joint Sealer, 705-2.03 Bridge Seals and 705-2.06 High Molecular Weight Methacrylate (HMWM) Resin of Section 705 Joint Materials and replace with the following:

705-2.02 JOINT SEALER.

Silicone Joint Sealer	ASTM D 5893

Hot Pour Joint Sealer (Asphalt, Concrete)	ASTM D6690, Type IV

705-2.03 BRIDGE SEALS.

1.	Preformed Strip Seals and Compression Seals. Use preformed seals constructed with only virgin natural polyisoprene (natural rubber) as the raw polymer in the elastomeric compound. Do not use polychloroprene (neoprene). Use steel extrusions meeting ASTM A709 Grade 36. Galvanize steel extrusions in accordance with Subsection 716-2.07. Use preformed material meeting the following requirements of ASTM D2000:

M4AA 514 A13b13c12f17

Use a lubricant-adhesive for installing preformed strip seals and compression seals meeting ASTM D4070.

a.	Certification. Furnish a Certified Test Report from the manufacturer or an independent testing laboratory containing a list of dimensional, chemical, metallurgical, electrical, physical, and other required test results of the specified material certifying that the product or assembly has passed all specified tests. Include the following:

(1)	the project name and number;

(2)	the manufacturer's name;

(3)	the name of the product or assembly;

(4)	a complete description of the material;

(5)	country of origin;

(6)	the lot, heat, or batch number that identifies the material;

(7)	all required test results for the specified material from the same lot, heat, or batch defined in Subsection 705-2.03.1.a.(6);

(8)	a statement, signed by a person having legal authority to act for the manufacturer or the independent testing laboratory, that the test results show that the product or assembly to be incorporated into the project has been sampled and tested and the samples have passed all specified tests.

Tag, stencil, stamp, or otherwise mark all materials or assemblies furnished under certification to the project with the lot number, heat number, batch number, or other appropriate identification, which can be readily recognized and legible, and is identical to the accompanying Certified Test Report.

2.	Silicone Expansion Joint Seals. Use materials that conform to the following:

a.	Silicone Joint Sealants.

(1)	Horizontal Joints.  Use formed-in-place sealant composed of 100 percent silicone that is self-leveling, cold applied, and two-part formulation meeting the requirements in Table 705-1.

(2)	Vertical Joints.  Use formed-in-place sealant composed of 100 percent silicone meeting the requirements of ASTM D5893, Type NS (Non-Sag). Do not use acid cure sealants.  Ensure the silicone sealant is compatible with the surface to which it is applied.

b.	Bond Breaking Backing Material. Use closed-cell expanded polyethylene foam backer rod meeting the requirements of ASTM D5249.

TABLE 705-1

SELF-LEVELING SEALANT REQUIREMENTS

| Property | Requirements | Test Method |
| --- | --- | --- |
| Extrusion Rate | Min, 50 mL/minute | ASTM C1183 |
| Specific Gravity | Min. 1.25 Max. 1.35 | ASTM D792 |
| Joint Elongation | Min. 600% | ASTM D5329 (modified)* |
| Joint Modulus (at 100% elongation) | Min. 3 psi Max. 12 psi | ASTM D5329 (modified)* |

*	Modify the ASTM D5329 test by using a pull rate of 2 inches per minute and a joint size of 1/2 inch x 1/2 inch x 2 inch.

705-2.06 EXPANDED POLYETHYLENE. Use closed-cell expanded polyethylene with a density of at least 2.1 lb/ft3 as determined by ASTM D3575 and with a minimum compressive stress of 9 psi at 25% deflection as determined by ASTM D3575.

SSP25-010116