SECTION 706
CONCRETE AND PLASTIC PIPE

Sect 706: Section Specials CR706.1. CR706.1 Replaces SSP11. CR706.1 will be further reviewed when SSHC 2016 is issued.

Related Sect/Sp:

Special Provisions

Replace Subsection 706-2.06:

706-2.06 PLASTIC PIPE. Non-perforated, semi-rigid, smooth-wall pipe meeting the following:

Polypropylene (PP)	AASHTO M330, Type S or Type D, ASTM F2736,

ASTM F2764

Polyethylene (PE)	AASHTO M 294, Type S or Type D

Polyvinyl Chloride (PVC) 	AASHTO M 264 or M 278

Acrylonitrile-Butadine-Styrene (ABS)	AASHTO M 264

Add Subsection 706-2.07:

706-2.07 CORRUGATED POLYETHYLENE PIPE. Meet the following:

Culverts	AASHTO M 294, Type S or Type D

Underdrains	AASHTO M 252

Add Subsection 706-2.09:

706-2.09 POLYPROPYLENE PIPE. Meet the following:

Storm	AASHTO M330, Type S or Type D, ASTM F2736 or ASTM F2764

Culvert	AASHTO M330, Type S or Type D, ASTM F2736 or ASTM F2764

Sanitary	ASTM F2736 or ASTM F2764

CR706.1-010116