SECTION 710
FENCE AND GUARDRAIL

Sect 000: SM5 2.04 only included in CR710.3. Replaces subsection.

Related Sect/Sp:

CR710.3. All projects with guardrail

Special Provisions

Replace Subsection 710-2.04 with the following:

710-2.04 METAL BEAM RAIL.

1.	W-Beam and Thrie Beam Guardrail.  Meet AASHTO M 180, Class A, Type II.

2.	Box-Beam Guardrail.  Meet:

a.	ASTM A500 Grade B, or

b.	ASTM A501.

Galvanize the rail per AASHTO M 111 after fabrication.

CR710.3-122217