Special Provisions

Replace Section 722 with the following:

SECTION 722
BRIDGE RAILING

Sect 722: Section Specials: SSP32. SSP32 will be further reviewed when SSHC 2016 is issued.

Related Sect/Sp:  507

722-2.01 BRIDGE RAILING.

Steel tube rail elements	ASTM A500, Grade B

Steel Thrie Beam elements	AASHTO M 180, Class B, Type II

Posts	ASTM A709, Grade 36

Machine bolts, cap screws, nuts and washers	ASTM A307

High strength bolts, nuts and washers	Subsection 716-2.03

Anchor bolts	AASHTO M 314, Grade 105; ASTM F1554,

Grade 105; or ASTM A449, Type 1

Anchor studs	AASHTO M 169, Grade 1015 or 1020

Shims, plates, angles and sleeves	ASTM A709, Grade 36

Galvanize steel portions of railing	AASHTO M 111 or M 232 and Subsection after fabrication.	716-2.07

722-2.02 CERTIFICATION. Furnish a certified test report from the manufacturer or an independent testing laboratory containing a list of dimensional, chemical, metallurgical, electrical, physical, and other required test results of the specified material certifying that the product or assembly has passed all specified tests. Include the following:

1.	the project name and number

2.	the manufacturer's name

3.	the name of the product or assembly

4.	a complete description of the material

5.	country of origin

6.	the lot, heat, or batch number that identifies the material

7.	all required test results for the specified material from the same lot, heat, or batch defined in Subsection 722-2.02.6

8.	a statement, signed by a person having legal authority to act for the manufacturer or the independent testing laboratory, that the test results show that the product or assembly to be incorporated into the project has been sampled and tested and the samples have passed all specified tests.

Tag, stencil, stamp, or otherwise mark all materials or assemblies furnished under certification to the project with the lot number, heat number, batch number, or other appropriate identification, which can be readily recognized and legible, and is identical to the accompanying certified test report.

SSP32-010116