SECTION 505
PILING

Sect 505: CR505.1

Related Sect/Sp:  504/CR504.1, 660/CR660.1, 668/CR668

Related Sect/Sp:

Special Provisions

505-3.04 SPLICES, EXTENSIONS, AND BUILD-UPS. Add the following:

CR505.1, use with high tower lighting.

High Tower Piling.

Field splices shall be located a minimum of 10 ft. from either end of the pile and limited to one per 40 ft. of pile length. Make the splice with a complete-joint-penetration groove weld with backing ring.

1.	Joint Preparation.

Cut off pile perpendicular to the pile centerline, "freehand" cutting is prohibited. Before welding, prepare pile top establishing the proper groove angle with a pipe beveller.  Touch up and repair surfaces to be welded by grinding. Clean pile ends inside and out for a width of 4 inches perpendicular to the groove, for the length of the groove, each side of the groove removing all moisture, grease, rust, mill scale, and other material that might negatively influence the weld quality.

2.	Weld Inspection.

a.	Visual Inspection (VT)	100%

b.	Ultrasonic Testing (UT)	100%

Inspection and testing by a third party American Welding Society (AWS) Certified Weld Inspector (CWI) qualified to perform Nondestructive Examination (NDE) of welds.

505-5.01 BASIS OF PAYMENT. Add the following:

Pay Item 505(20) is a new and separate pay item. This is to permit more than one pay item number for multiple pile types on the same project. Numbers will need to be coordinated and added to aashtoware.

Pay Item 505(20) Furnish and Install High Tower Lighting Piles includes the costs for both furnishing and installing piles for high tower lighting in Pay Item 668(1) High Tower Lighting System Complete.

Add the following Pay Items:

Pay Item No.	Pay Item	Pay Unit

505(20)	Furnish and Install High Tower Lighting Piles	Each

CR505.1-100118