SECTION 632
PAVING FABRIC

Sect 632

Related Sect/Sp: 619, 630, 631, 633, 634, 641, 727, 729

Special Provisions

632-3.01 CONSTRUCTION.

2.	Application of Sealant. Replace the 2nd Sentence with:  Apply the asphalt sealant uniformly at 0.20 to 0.30 gallons per square yard and at a temperature of between 295 F min. and 320 F max. in the distributor tank, or as directed by the Engineer and/or Paving Fabric manufacturer.

4.	Fabric Placement. Add the following: Overlap geotextile joints to ensure full closure of the joint. Do not exceed a 6 inch overlap. Do not allow the Geotextile to become wet. Removal and replacement of damaged geotextiles is the responsibility of the Contractor.

5.	Bituminous Surface Course Overlay. Add the following: Do not allow the temperature of the hot-mix asphalt to exceed manufacturer's recommendations.

632-4.01 METHOD OF MEASUREMENT. Add the following:  No allowance will be made for overlap, whether at joints or patches.

632-5.01 BASIS OF PAYMENT. Add the following: Removal and replacement of damaged geotextiles is subsidiary to the Section 632 Pay Items.

CR632.1-070115