SECTION 705
JOINT MATERIAL

Sect 705: CR705.1

Related Sect/Sp:  602/CR602.1, 603/CR603, 605/CR605.1, 706/CR706.1

Special Provisions

Replace Subsection 705-2.05 with the following:

705-2.05 FLEXIBLE WATERTIGHT GASKETS. Ring gaskets (seals):

1.	Joining rigid concrete (cast-in-place and precast) pipes, manholes, box sections and other structures:

a.	ASTM C443 Specification for Joints for Concrete Pipe and Manholes, Using Rubber Gaskets

b.	ASTM C990 Specification for Joints for Concrete Pipe, Manholes, and Precast Box Sections Using Preformed flexible Joint Sealants (Butyl Rubber Sealant)

c.	ASTM C1628 Specification for Joints for Concrete Gravity Flow Sewer Pipe, Using Rubber Gaskets

d.	ASTM C1619 Specification for Elastomeric Seals for Joining Concrete Structures

Class B (oil resistant performance)

2.	Joining flexible metal pipe (steel and aluminum):

a.	ASTM C443 Specification for Joints for Concrete Pipe and Manholes, Using Rubber Gaskets

b.	ASTM C1619 Specification for Elastomeric Seals for Joining Concrete Structures

Class B (oil resistant performance)

c.	ASTM D1056 Specification for Flexible Cellular Materials-Sponge or Expanded Rubber

(1)	Type 2-Closed cell rubber

(2)	Class B-Oil resistance with low mass change

(3)	Grade 3-Compression-deflection range from 9 to 13 psi

Use continuous flat gaskets with thickness 1/2-inch greater than the nominal depth of the corrugation for bands with projections or flat bands and 3/8-inch for corrugated bands.

3.	Joining plastic pipe:

a.	ASTM D3212 Specification for Joints for Drain and Sewer Plastic Pipes Using Flexible Elastomeric Seals

b.	ASTM F477 Specification for Elastomeric Seals (Gaskets) for Joining Plastic Pipe

Not less than 50% by volume oil resistant polymer

CR705.1-010119