SECTION 710
FENCE AND GUARDRAIL

Sect 710: CR710.2.  (CR710.2-020119 combines HSM18-2 with CR requirements)

Related Sect/Sp:  606/CR606/CR606.9.10.13.  (CR606 replacement special for SSHC Section 606. Add CR606.9.10.13, as applicable)

CR710.2.3. All projects with guardrail.

Special Provisions

Replace Subsection 710-2.04 with the following:

710-2.04 METAL BEAM RAIL.

1.	W-Beam and Thrie Beam Guardrail. Meet AASHTO M 180, Class A, Type II. Galvanize after fabrication. Meet the coating requirements of AASHTO M 180 9, Type II Beams and AASHTO M 111 (ASTM A123) as referenced.

2.	Box-Beams Guardrail. Meet:

a.	ASTM A500 Grade B, or

b.	ASTM A501.

Galvanize after fabrication. Meet the coating requirements of AASHTO M 111 (ASTM A123).

CR710.3-020119

Replace Subsection 710-2.11 with the following:

710-2.11 GUARDRAIL TERMINALS.

Corrugated sheet steel beams for highway guardrail meet the requirements of AASHTO M 180, Class A, Type II. Galvanize after fabrication. Meet the coating requirements of AASHTO M 180 9, Type II Beams and AASHTO M 111 (ASTM A123) as referenced.

Iron and steel products made from rolled, pressed and forged shapes, castings, plates bars, and strips galvanize after fabrication. Meet the coating requirements of AASHTO M 111 (ASTM A123).

Iron and steel hardware galvanize after fabrication. Meet the coating requirements of AASHTO M 232 (ASTM A153).

Provide the following terminal type, as shown on the plans, for single-rail W-beam guardrail.

Parallel Terminal.

1.	Crashworthiness: Mash 16 compliant Test Level 3 terminals. Submit FHWA eligibility letter.

2.	Length: 50 feet.

3.	End Offset: 0 to 2 feet (25:1 or flatter straight taper). Offset end as shown on the plans.

4.	Manufacturers.

a.	Road Systems, Inc.	Model: MSKT

2616 Old Howard County Airport

Big Spring, Texas 79720

Ph: (432) 263-2435.

b.	Trinity Highway Products, L.L.C.	Model: Soft-Stop

950 West 400 south

Centerville, Utah 84014

Ph: (801) 292-4461

c.	Approved equivalent

5.	Retroreflective Sheeting for Terminals.

a.	ASTM D4956 Type III, IV, or V (1.0 square foot, minimum)

b.	Yellow and black bars sloping 45 degrees downward toward the traffic side

c.	Place on the end section

CR710.2-020119