SECTION 301
AGGREGATE BASE AND SURFACE COURSE

Special Provision

Sect 301:  C301.1.2.3.HSM20.5- 20.1130-1	Related Sect/Sp:  608/C608.1.2, C703/C703.1

C301.1 substituting Ram for aggregate base course; C301.2 use of "Layton Box" in sidewalks and pathways;

C301.3 add glass in base course. HSM20.5-113020-1 insert in all projects that include work related to Section 301.

301-2.01 MATERIALS.

Add the following after the first sentence:

Recycled Asphalt Material (RAM) may be substituted for aggregate base course, inch for inch, if the following conditions are met:

1.	RAM shall be crushed or processed to 100 percent by weight passing the 1.5-inch sieve and 95-100 percent by weight passing the 1-inch sieve.

2.	The gradation of the extracted aggregate shall meet the following:

TABLE 301-2.01-1

EXTRACTED AGGREGATE GRADATION

| Sieve | Percent Passing by Weight |
| --- | --- |
| 1-inch | 100 |
| 3/4-inch | 70 – 100 |
| 3/8-inch | 42 – 90 |
| No. 4 | 28 – 78 |
| No. 16 | 11 – 54 |
| No. 50 | 5 – 34 |
| No. 100 | 3 – 22 |
| No. 200 | 2 - 12 |

3.	The asphalt content shall be 2.5 – 5.0 percent by weight of the RAM.

C301.1-07.0124-1

301-3.01 PLACING.

Add the following:

Place base course material, used for the sidewalk and pathway foundations, with equipment capable of providing a specified depth and uniform surface.

C301.2-16.0621

Add No. 5 after the 5th paragraph:

5.	within 50 feet of detector loops.

C301.3-15.0220

Standard Modification

301-3.03 SHAPING AND COMPACTION.

In the second paragraph delete "and ATM 214".

HSM20.5-20.1130-2

Add the following:

If recycled asphalt material is substituted for aggregate base course, the following conditions shall be met:

1.	Density acceptance will be determined by control strip method ATM 412.  Use a test strip with a vibratory compactor with a minimum dynamic force of 40,000 pounds.  The optimum density will be determined by the Engineer using a nuclear densometer gauge to monitor the test strip.  Adequate water shall be added to aid compaction.

2.	After the appropriate coverage with the vibratory compactor, a minimum of 6 passes with a pneumatic tire roller shall be completed.  Tires shall be inflated to 80 psi ( 5 psi) and the roller shall have a minimum operating weight per tire of 3,000 pounds.

301-5.01 BASIS OF PAYMENT.

Add the following:

Recycled asphalt material substituted for aggregate base course will be paid for as Item 301.0001.____ Aggregate Base Course, at the unit price shown in the bid schedule for that Item.

C301.1-07.0124-1