section 501
CONCRETE FOR STRUCTURES

Standard Modification

Section 501: HSM20.23	Related Sect/Sp:

Apply to all projects with work related to Section 501

501-2.02 COMPOSITION OF MIXTURE – JOB MIX DESIGN.

Replace Table 501-4 with the following:

TABLE 501-4

AIR CONTENT REQUIREMENTS

| Class of Concrete | Air Content |
| --- | --- |
| A | 6.0% 0.5% |
| A-A | 6.0% 0.5% |
| P | 3.50% minimum1 and Super Air Meter (SAM) number 0.201 |
| DS | Not required |

1Not required for web and bottom flange of precast, prestressed decked bulb-tee girders.

HSM20.23-123121