SECTION 505
PILING

Special Provisions

Sect 505: CR505.1.2.	CR505.1 hightower lighting.

Related Sect/Sp: 504/CR504.1, 660/CR660.1, 668/CR668 (future high tower special)

505-3.04 SPLICES, EXTENSIONS, AND BUILD-UPS.

Add the following:

High Tower Piling.

Field splices shall be located a minimum of 10 ft. from either end of the pile and limited to one per 40 ft. of pile length. Make the splice with a complete-joint-penetration groove weld with backing ring.

1.	Joint Preparation.

Cut off pile perpendicular to the pile centerline, "freehand" cutting is prohibited. Before welding, prepare pile top establishing the proper groove angle with a pipe beveller.  Touch up and repair surfaces to be welded by grinding. Clean pile ends inside and out for a width of 4 inches perpendicular to the groove, for the length of the groove, each side of the groove removing all moisture, grease, rust, mill scale, and other material that might negatively influence the weld quality.

2.	Weld Inspection.

a.	Visual Inspection (VT)	100%

b.	Ultrasonic Testing (UT)	100%

Inspection and testing by a third party American Welding Society (AWS) Certified Weld Inspector (CWI) qualified to perform Nondestructive Examination (NDE) of welds.

505-5.01 BASIS OF PAYMENT.

Add the following:

Pay Item 505.2003.____ High Tower Lighting Piles, Furnish and Install, includes the costs for both furnishing and installing piles for high tower lighting in Pay Item 668.2000.____ High Tower Lighting System Complete.

Add the following Pay Items:

| pay item |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 505.2003.____ | High Tower Lighting Piles, Furnish and Install | Each |

CR505.1-100118R