SECTION 505
PILING

Special Provisions

Sect 505: C505.1.2.HSM20.54-25.0303	C505.1 Hightower Lighting	Related Sect/Sp: 504/C504.1, 660/C660.1, 668/C668 (future high tower special)

C505.2 Hwy lighting. Lighting standard requirements are for typical soil conditions. Address soil conditions where 15 ft embedment is insufficient, peat, etc.

505-3.03 DRIVING PILES.

Replace the 1st sentence in the 1st paragraph with the following:

Drive all piles, except piles for lighting standards, to the driving resistance and minimum penetration specified in the Contract documents using the pile driving criteria provided by the Engineer.

Add No. 5:

5.	Piles for Lighting Standards. For lighting standards, install piles of sufficient length to cut the pile at the required cut-off elevation and to provide the minimum installed length shown on the Plans.

Sites for lighting standard foundations can contain subsurface soils that consist of very dense sandy gravel with cobbles and boulders.

When the minimum pile length, shown on the Plans, for a lighting standard foundation cannot be achieved, install the pile tip to an elevation established by the Engineer.

C505.2-18.1001-1

505-3.04 SPLICES, EXTENSIONS, AND BUILD-UPS.

Add the following:

High Tower Piling.

Field splices shall be located a minimum of 10 ft. from either end of the pile and limited to one per 40 ft. of pile length. Make the splice with a complete-joint-penetration groove weld with backing ring.

1.	Joint Preparation.

Cut off pile perpendicular to the pile centerline, "freehand" cutting is prohibited. Before welding, prepare pile top establishing the proper groove angle with a pipe beveller.  Touch up and repair surfaces to be welded by grinding. Clean pile ends inside and out for a width of 4 inches perpendicular to the groove, for the length of the groove, each side of the groove removing all moisture, grease, rust, mill scale, and other material that might negatively influence the weld quality.

2.	Weld Inspection.

a.	Visual Inspection (VT)	100%

b.	Ultrasonic Testing (UT)	100%

Inspection and testing by a third party American Welding Society (AWS) Certified Weld Inspector (CWI) qualified to perform Nondestructive Examination (NDE) of welds.

505-5.01 BASIS OF PAYMENT.

Add the following:

Pay Item 505.2003.____ High Tower Lighting Piles, Furnish and Install, includes the costs for both furnishing and installing piles for high tower lighting in Pay Item 668.2000.____ High Tower Lighting System Complete.

| PAY ITEM |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 505.2003.____ | High Tower Lighting Piles, Furnish and Install | Each |

C505.1-18.1001-1

Add the following:

Pay Item 505.2004.____ Lighting Standard Piles, Furnish, and Install, includes the costs for both furnishing and installing piles for lighting standards for Pay Item 660.0003.____ Highway Lighting System Complete.

| PAY ITEM |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 505.2004.____ | Lighting Standard Piles, Furnish and Install | Each |

C505.2-18.1001-1

Standard Modification

Replace the Pay Item table with the following:

Payment will be made under:

| PAY ITEM |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 505.0005.0000 | Furnish Structural Steel Pipe Piles, ____ | LF |
| 505.0005.0001 | Furnish Structural Steel H-Piles, ____ | LF |
| 505.0006.0000 | Drive Structural Steel Pipe Piles, ___ | Each |
| 505.0006.0001 | Drive Structural Steel H-Piles, ____ | Each |
| 505.0009.____ | Structural Steel Piles | SF |
| 505.0014.____ | Special Pile Excavation | CS |

HSM20.54-25.0303f