section 550

commercial concrete

Standard Modification

Section 550: CR550.HSM20.8-113020	Apply to all projects with work related to Section 550

Related Sect/Sp: 501, 503

550-2.02 COMPOSITION OF MIXTURE – JOB MIX DESIGN.

Replace Table 550-1 with the following:

TABLE 550-1

COMMERCIAL CONCRETE DESIGN REQUIREMENTS

| Class | B-B | B | W |
| --- | --- | --- | --- |
| Water-Cement Ratio, lbs/lbs, maximum | 0.40 | 0.45 | 0.50 |
| Total Air Content, % | 5.5 – 6.5 | 5.5 – 6.5 | 4.0 – 6.5 |
| Coarse Aggregate Gradation, AASHTO M43a. | No. 57 or 67 | No. 57 or 67 | No. 7, 8, 57, or 67 |
| Compressive Strength, psi, minimum | 5,000 | 4,000 | 3,000 |

a.	Alternative sizes of coarse aggregate, as shown in AASHTO M 43, may be used when approved in writing.

550-5.01 BASIS OF PAYMENT.

Replace the first sentence with the following:

If items 550.0001.____, 550.0002.____, 550.0003.____, 550.0004.____, 550.0005.____, or 550.0006.____ do not appear in the Bid Schedule concrete is subsidiary to other items.

Add the following pay items:

| pay item |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 550.0005.____ | Class B-B Concrete | LS |
| 550.0006.____ | Class B-B Concrete | CY |

CR550.HSM20.8-113020R