Sect 608:	CR608 for special asphalt and concrete surfaces incorporates both the SSHC Section 608 with CR608.1 and HSM20.10-113020

Related Sect/Sp:  401/CR401, 703/CR703.1

SECTION 608, SIDEWALKS	 - CR608	Notes to Designer and Engineer

CR608.2 addresses concrete and asphalt (HMA) work for pavement, sidewalks, borders, plazas, pathways, medians, roundabouts (special concrete and HMA) and similar.  Addressed are the finishes, broom, aggregate, color, pattern imprinting, and painting and is a complete replacement for the SSHC Section 608 incorporating the unchanged portions of the SSHC specification.

	Not recommended to use patterned and painted asphalt. Increase the thickness for the pattern imprint if used.

	Recommend reinforcing all concrete slabs.

	Make concrete medians 6" thick minimum, reinforce, and apply colorant and imprinting.

	Make concrete roundabouts 6" thick minimum, pay special attention to reinforcing, control, and construction joints.

Reinforcing

Reinforcing for the typical slab (sidewalk) is noted here for inclusion in the special when applicable.  Construction generally does not reinforce the 4 inch sidewalk.  The 4" slab reinforcing noted here differs from that noted for the "special concrete" slabs.  It is based on the least requirement, not the most applicable.  The 6 inch slab is the same as for the "special concrete" slab.

| Thickness | Reinforcing |
| --- | --- |
| 4 Inch | #3 @ 18" O.C. Each Way or 6x6 - W1.4xW1.4 |
| 6 inch | #5 @ 12" O.C. Each Way |

Color and Pattern Imprinting

The order of precedence for selecting the color and pattern is (similar for HMA):

1.	Use a color and pattern similar to other surrounding or nearby pattern imprinted concrete.

2.	Use a color & pattern as required meeting project specific required theme.

3.	Use a typical color, a color used on other state projects.

Past project colors and patterns, include:

| Imprint System | Pattern | Integral Color | Hardener | Release Agent | Cure Agent | Sealer |
| --- | --- | --- | --- | --- | --- | --- |
| Curb Ramps |  | Davis Color: #160, Red Brick |  |  |  |  |
| Brickform | European Fan, TM-400 | Chromix: Sorrento Red, ASTM C979 & 494 | Bomanite: Franciscan Red, Heavy Duty | Compatible with Colorant Manufacturer | Bomanite; Membrane Color Cure ASTM C309 | Bomaseal, C-18 |
| Bomanite | Belgian Block | Bomanite: Thistle Brown | Bomanite: Caramel |  |  |  |
| Bomanite | Herringbone Brick | Bomanite: Red Clay | Bomanite: Franciscan Red |  |  |  |
| Bomanite | Running Bond, Brick | Bomanite: Red Clay | Bomanite: Heavy Duty |  | Bomanite | Bomanite |
| Bomanite | Running Bond, Regular slate | Bomanite: Apricot | Bomanite: Harvest Amber | Bomanite: Liquid Release Agent | Bomanite: Con-Shield | Bomanite: Hydrolock |
| Bomanite | Fish Scale | Bomanite: Red Clay & Brick Red, ASTM C979 & C494 | Bomanite: Heavy Duty | Bomanite: Compatible w/ Colorant Manufacturer | Bomanite: Membrane Color Cure, ASTM C309 | Bomaseal, C-18 |
| Bomanite | 8x8 Running Bond, Regular Slate | Color Type A. Scofield: Dusty Mauve; Interstar: Redwood Color Type B. Scofield: Autumn Beige; Interstar: Champagne |  | Color Type A. Brickform: Antique, 650 Smokey Blue; Bomanite: Cobblestone Gray Color Type B. Brickform: Antique, 350 Desert Tan; Bomanite: Harvest Amber |  |  |
| Bomanite. Cobblecrete Int. Art Crete Inc. | Running Belgian Block. Running Cobblestone. Faux Brick. | Davis Color: #160, Red Brick | Davis Color or Scofield; Terra Cotta or Mexican tile |  |  |  |
| Bomanite/ Bomacron Imprinting Tools | Running Bond, Brick | Bomanite: Red Clay; Davis Color: #160, Red Brick | Bomanite: Franciscan Red | Bomanite: Liquid Release | Bomanite: Con-Shield | Bomanite: Hydrolock |
| Asphalt Pattern Imprinting: | Medians & Pathways Offset Brick, Create Tool | FED. Std. 595, Color 30111, Standard Brick Red, Two-part epoxy |  |  |  |  |

Aspen Leaf Pattern (Aspen Leaf Flexible Mat Stamp) may be owned by the State…

Replace Section 608 with the following:

SECTION 608
SIDEWALKS

Special Provisions

608-1.01 DESCRIPTION. Construct, or retrofit asphalt, or concrete sidewalks.

Sidewalk Section 608 includes "sidewalks", pathways, medians, curb ramps, miscellaneous on-grade concrete, and asphalt surfaces not addressed elsewhere in the specifications.

608-2.01 MATERIALS. Use materials that conform to the following:

1.	Concrete

Bed Course Material	Subsection 703-2.03

Joint Fillers	Subsection 705-2.01

Joint Sealers	Subsection 705-2.02

Concrete	Section 550, Class B

Acid Wash	Muriatic or Phosphoric

Admixtures	AASHTO M 194 Chemical Admixtures†

ASTM C 494 Standard Specification for Chemical Admixtures for Concrete†

Curing Agents	ASTM C 309, Liquid Membrane-Forming Compounds for Curing Concrete †

Expansion Joints	AASHTO M-33 Preformed Expansion Joint Filler for Concrete (Bituminous Type)

Integral Color Agent	ASTM C 979 Standard Specification for Pigments for Integrally Colored Concrete

Reinforcing Steel	Section 503

†	Compatible with colorant manufacturer.

Provide concrete for slabs according to Section 501, ACI 303R, 303.1, this specification and the material manufacturer's and supplier's written instructions.

Maximum slump 4-inch, except 8-inch maximum if using super plasticizers or mid-range water reducers. Mix used for sample(s) shall be the same as the production mix(s).

Concrete - Exposed Aggregate Finish. Provide aggregate from a single source.  Keep aggregate for exposed aggregate finish separate from other project aggregate.

Concrete – Colored. Color concrete using an integral color, with a surface hardener, a color cure, a release agent, and a sealer compatible with colorant(s).

Concrete - Pattern Imprinted. Use a manufactured system designed to provide the pattern specified and a release agent compatible with the colorant.

2.	Asphalt (HMA)

Bed Course Material	Subsection 703-2.03

Asphalt Binder, PG 52-28	Subsection 702-2.01

Aggregate, Type II or III	Subsection 703-2.04

Mix Design Requirements (ATM 417)

Marshall Stability, pounds, min.	1000

Percent Voids, Total Mix	2-5

Compaction, Blows/side	50

Coating/Paint:

Material - Methyl Methacrylate (MMA)	Subsection 712-2.17 (MMA only)

Color	Federal Standard 595, color 30111 (Brick Red)

3.	Detectable Warnings

Cast iron detectable warning plates with truncated dome pattern, a slip resistant surface, and with handle or flange on bottom or approved equal. Detectable warning plates shall be coated with yellow polymer soaked finish. Detectable warnings shall be manufactured according to the 2006 U.S. DOT ADA Standards for Transportation Facilities.

608-2.02 REFERENCES.

1.	ACI 303		Cast-In-Place Architectural Concrete Practice

2.	PCA PA124		Finishing Concrete Slabs with Color and Texture

3.	PCA SP021		Color and Texture in Architectural Concrete

608-2.03 SUBMITTALS – EXPOSED AGGREGATE, COLORED CONCRETE, PAINTED HMA AND PATTERN IMPRINTED CONCRETE AND HMA.  Provide complete submittals (3 printed copies, except samples as specified below), to the Engineer for review and approval, at least 21 days before beginning construction of concrete and asphalt items.  Submittals will be returned to the Contractor within 14 days from the date submitted, marked as approved by the Department, or requiring revisions.  Amend and resubmit the documents for review until approved by the Engineer.  Receive approval before beginning production.

Submit shop drawings, product data, specifications, certifications; manufacturers and installer's resumes, and samples as specified in Section 401, 501, 503, 608 and herein.

1.	Shop Drawings, Product Data, Specifications, and Certifications.

a.	Exposed aggregate finish:  manufacturer's chemical surface retarder.

b.	Integral concrete colorant:  manufacturer's color chart, and chipset.  Indicate color additive numbers and required dosage rates as part of the concrete mix submittal, Subsection 501-3.01.

c.	Manufacturer's concrete pattern imprinting system.

d.	Manufacturer's fabricated HMA pattern imprinting tool - shop drawings.

e.	Methyl Methacrylate for coating HMA.

f.	Other when requested by the Engineer.

2.	Resumes.

a.	Manufacturer.

Concrete. Provide documentation for five years of successful product performance, with a minimum of five completed projects and including but not limited to:

	Manufacturer's colorant, hardener, color cure, release agent, and sealer

	Batch Plant's mixing of manufacturer's colorants and other additives, and product delivery

	Manufacturer's pattern imprinting system

HMA. Provide documentation of two years and three projects successfully fabricating pattern imprinting tools and successful product performance applying MMA in similar applications to this Project.

b.	Installer.

Concrete and HMA. Installer(s) with 2 years' experience and 3 successfully completed projects of similar configuration and method of installation.

In addition:

1)	For projects with concrete integral colorant and or pattern imprint system, provide a minimum of one project using the proposed manufacturer's colorant and pattern imprint system.

3.	Manufacturer's.

Provide a minimum of 3 manufacturers.  Davis provides colorant only.

All manufacturers, listed and other, are required to submit for review and approval.

Manufacturers of concrete colorant and pattern imprinting systems:

| Bomanite Corporation P.O. Box 599 Madera, CA 93639 Ph: 303.369.1115 Fax: 303.291.0282 Email: bomanite.com | Brickform, division of Solomon Colors, Inc. 11061 Jersey Blvd. Rancho Cucamonga, CA 91730 Ph: 800.483.9628 Email: brickform.com | Davis Colors 3700 East Olympic Blvd. Los Angeles, CA 90023 Ph: 800.356.4848 Fax: 323.269.1053 Email: daviscolors.com | L.M. Scofield Company 6533 Bandini Blvd. Los Angeles, CA 90040 Ph: 323 720.3000 Fax: 323.720.3000 Email: Scofield.com |
| --- | --- | --- | --- |

4.	Pattern Imprinting, Coloring Concrete, and HMA Painting Plans.

Provide pattern imprinting, concrete coloring, and HMA painting plans to the Engineer for review and approval.  Include the following, at a minimum, to achieve a final product that accurately represents, to scale, colored concrete, painted HMA and the pattern imprinted concrete and HMA (including the joints) elements:

a.	the sequence and schedule of operations,

b.	the proposed method of pattern imprinting,

c.	the method of coloring the concrete,

d.	the method of applying the MMA coating/paint to the HMA.

5.	Exposed aggregate, Colored Concrete and Painted HMA and Pattern Imprinted Concrete and HMA Sample(s).

Provide one sample, equal to the width of the item, 6 ft x 6 ft maximum, 4 ft x 4 ft minimum, of each item for review by the Engineer.  Demonstrate exposing the aggregate, the addition of colorant to the concrete, painting the HMA and pattern imprinting the concrete and HMA on each sample provided.

Receive written approval of the sample prior to beginning production work.

Retain samples of binder(s), sand(s), aggregate(s), and color additive, used in the sample for comparison with the item production materials.  Keep sample through completion of related work for use as a quality standard for finished work.  Keep the sample through Project completion when requested by the Engineer.

CONSTRUCTION REQUIREMENTS

608-3.01 CONCRETE SIDEWALKS. Excavate to the required depth and to a width necessary to install and brace the forms. Shape and compact the foundation to a firm, even surface conforming to the section shown on the Plans. Replace soft and yielding material with approved material. Compact bed course material according to Subsection 203-3.04.

Use full depth forms made of wood or metal. Use forms that are straight, free from warp, and strong enough to resist the pressure of the concrete without springing. Coat forms with an approved form-release agent. Brace and stake the forms so that they maintain their position until their removal.

Thoroughly moisten the foundation immediately before placing the concrete.

Finish the surface according to Section 550-3.05. Do not plaster the surface. Edge all outside slab edges and all joints to a 1/4 inch radius.

Make expansion joints to the dimensions and spacing shown on the Plans and fill with the type of preformed expansion joint fill specified.

Divide the sidewalk into specified sections using dummy joints formed by a jointing tool or other acceptable means. Make dummy joints 1/3 the depth of the concrete and approximately 1/8 inch wide.

Form construction joints around all appurtenances such as manholes, utility poles, buildings, or bridges, extending into and through the sidewalk. Install preformed expansion joint filler 1/2 inch thick in construction joints. Extend the expansion joint material the full depth of the walk.

Apply joint sealer evenly to completely seal all joints.

Cure the concrete according to Section 550-3.06. During the curing period, exclude all pedestrian and vehicular traffic. Exclude vehicular traffic for additional time as directed.

The Engineer will test the finished surface with a 10-foot straightedge. Variations of more than 1/4-inch from the edge of the straightedge across or along the sidewalk surface, except at grade changes, are unacceptable. Portions of the sidewalk surface and pedestrian ramps less than 10 feet in width, or length may be tested using a shorter straightedge.

Exposed Aggregate, Colored Concrete and Painted HMA and Pattern Imprinted Concrete and HMA

Match the Project work to the approved sample.  Significant differences in appearance (texture, color, pattern, or other) between adjacent panels/sections of work, from the approved sample including adjacent panels/sections similar to the approved sample yet significantly different to each other, as judged by the Engineer, will result in removal and replacement of the deficient panel(s)/section(s) of work.

Take all precautions to avoid damaging new and existing, concrete and asphalt.

Prevent surrounding materials from being discolored by the concrete and HMA and the HMA MMA coating (curbs, gutters, and other).  When directed by the Engineer, in writing, remove stains and coatings on other concrete and or HMA, resulting from your work.

Where HMA paving is against; exposed aggregate finish, colored, pattern imprinted; colored and pattern imprinted concrete, place the concrete prior to asphalt paving.  Do not place the HMA pavement until the concrete has cured sufficiently to prevent damage from the paving operation.

Acceptance of corrective work requires the Engineer's written approval.  Repair all new and existing damaged concrete and HMA, including the removal of surface contaminants, to the satisfaction of the Engineer.  The Engineer will not provide written approval until all damaged concrete and HMA is repaired.

1.	Slab Types.

Indicate the slab type in the Plans.  Roundabouts will require specifics to be addressed including reinforcing…,

Roundabout example: HSIP: Johns Road and Klatt Road Intersection Improvements, Z545990000 See drawings and specifications.

| TABLE 608-1 Slab Type Requirementsa, b |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Typec | Description | Finishd, e, f | Added Colorg | Added Patterng | th Inches | Reinforcingi (bar spacing each way) |
| a. & b. | Typical | Broom |  |  | 4, 6 |  |
| I | Broom | Broom |  |  | 4 | 4x4  W2.9xW2.9 |
|  |  |  |  |  | 6 | #5@12" O.C. |
|  |  |  |  |  | 8 | #6@12" O.C. |
| II | Exposed Aggregate | Aggregate |  |  | 4 | 4x4  W2.9xW2.9 |
|  |  |  |  |  | 6 | #5@12" O.C. |
| III | Colored | Broom | Color Manufacturer |  | 4 | 4x4  W2.9xW2.9 |
|  |  |  |  |  | 6 | #5@12" O.C. |
| IV | Pattern Imprinted | Coordinate |  | Pattern Manufacturer | 4 | 4x4  W2.9xW2.9 |
|  |  |  |  |  | 6 | #5@12" O.C. |
| V | Colored & Pattern Imprinted | Coordinate | Color & Pattern Manufacturer |  | 4 | 4x4  W2.9xW2.9 |
|  |  |  |  |  | 6 | #5@12" O.C. |
| a. Sealer and Hardener: provide for all slabs. Include the typical sidewalk approach detail in the Plans b. Transition the slab at approaches as shown in the plans. c. Type a. & b.; Pay Items 608.0001.____, are the "Typical" concrete sidewalk. d. Broom: provide a medium broom finish. e. Aggregate: provide a uniform color slightly darker than the typical uncolored slab with a uniform reveal according to ACI 303.1. f. Coordinate: coordinate and provide finish as required by pattern imprint system manufacturer. g. Color and Pattern: provide color and or pattern similar to that noted and available from the listed manufacturer(s). Provide color and pattern from the same manufacturer or provide from different manufacturers with a certification from each permitting warranted use of their product with the product of the other manufacturer. Use a release agent as approved by the manufacturer(s). h. t: provide the slab thickness, denoted as "t" i. Reinforcing: Provide welded wire fabric in sheets not rolls. Lap joints 1 1/2 mesh minimum. |  |  |  |  |  |  |

2.	Joints.

Joints spacing, layout:  address joint spacing and layout in the Plans, if other than noted below.  Roundabouts will require specifics…

Lay out joints as shown or noted in the Plans and Specifications, if not shown or noted provide:

a.	Control Joints.  Maximum spacing equals 12 ft.  (also referred to as, "dummy joints")

(1)	the joint configuration should create a square or rectangle with the long side no more than 1.5 times the short side,

(2)	space the control joint matching the width of the slab,

(3)	at corners and intersections, align the joints parallel to the edge(s) of the intersecting slab.

(4)	locate the joints equally spaced between the:  ends/edges of slab, slab corners, slab intersections or a combination of one and another.

b.	Expansion Joints.  Maximum spacing equals 36 ft.

Touch up pattern and finish edges with hand tools immediately after placing concrete and as directed by the manufacturer(s) and Engineer.

608-3.02 ASPHALT SIDEWALKS. Place bed course material in layers. Compact it according to Subsection 203-3.04.

Place asphalt material on the compacted bed course in one or more courses as indicated on the Plans. Compact it uniformly to required depth. Use a power roller of an acceptable type and weight. In areas inaccessible to the roller, use other approved methods.

608-3.03 CURB RAMPS. Construct curb ramps according to the details and the locations shown on the Plans. Follow the construction requirements of Subsection 608-3.01. Install detectable warnings.

Measure curb ramp slopes with a 24-inch electronic level. Calibrate and operate the level according to the manufacturer's instructions.

Provide the slab Type as identified here and elsewhere, Type ___. Refer to 608-3.01.1 Slab Type, Table 608-1 Slab Type Requirements for further information.

Be sure to identify the curb ramp slab with the appropriate type from 3.01 above.

608-3.04 DETECTABLE WARNINGS. Construct detectable warnings according to the details and the locations shown on the Plans. Install detectable warning plates by embedding plate flanges into cast-in-place concrete construction so there are no vertical changes in grade exceeding 0.25 inch or horizontal gaps exceeding 0.5 inch. Align pattern on a square grid in the predominate direction of travel. Install the same type of detectable warning plate throughout the project.

Detectable warnings shall be installed according to the 2006 U.S. DOT ADA Standards for Transportation Facilities.

608-3.05 ASPHALT – PATTERN IMPRINTED AND PAINTED.  Construct pattern imprinted and painted HMA according to Subsection 608-3.02 Asphalt Sidewalks and as noted herein.

1.	Pattern.  Fabricate the imprint tool pattern to match standard brick dimensions in a running bond configuration with a slightly wider joint/indent spaced similar to the concrete expansion Joint.

2.	Painting.  Prepare the asphalt surface and apply the coating/paint according to the MMA manufacturer's instructions. Apply coating (MMA) completely covering the asphalt surface including pattern imprint.  Do not fill the pattern indentation, with MMA, flush with the top surface.  Leave a 1/8", smooth, concave painted/coated surface between bricks (joint).

608-4.01 METHOD OF MEASUREMENT. Section 109 and as follows:

Sidewalk by area of finished surface, weight of material placed, and lump sum as included in the bid schedule. Ramps are included in the measurement unless included as a separate measured and paid item.

HMA used for matching existing surfaces, such as paved parking lots behind a new sidewalk/pathway, will be included in the measurement of the related asphalt Pay Item.

608-5.01 BASIS OF PAYMENT.

Subsidiary to the Pay Items: excavation, backfill, reinforcement, expansion joint material, samples, asphalt binder, corrective work, and other related miscellaneous items.

Embankment and bed course materials will be furnished, placed, and paid under Sections 203 and 301, respectively.

Curb Ramp when included in the bid schedule includes ramp runs, backing curbs, flares, landings to provide a single street-level access and detectable warnings, except detectable warnings are paid separately when included as an item in the bid schedule.

| pay item |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 608.0001.___ | Concrete Sidewalk, 4 inches thick | SY |
| 608.0001.___ | Concrete Sidewalk, 6 inches thick | SY |
| 608.0002.___ | Asphalt Sidewalk | Ton |
| 608.0006.___ | Curb Ramp | Each |
| 608.0007.___ | Curb Ramp, Retrofit | Each |
| 608.2002.___ | Asphalt Pathway | Ton |
| 608.2004.___ | Asphalt Medians | Ton |
| 608.2006.___ | Asphalt Pathways and Medians | Ton |
| 608.2007.___ | Asphalt, (Sidewalk, Plaza, etc., __ Inches Thick) | SY |
| 608.2008.___ | Asphalt Pattern Imprinted and Painted, (Median, etc., __ Inches Thick) | SY |
| 608.2010.___ | Concrete Sidewalk Wall, (Type __; Slab __ in; Wall __ in; Ht __ ft) | LF |
| 608.2011.___ | Concrete Sidewalk Retaining Wall, (Type __; Slab __ in; Wall __ in; Ht __ ft) | LF |
| 608.2012.___ | Concrete Sidewalk Barrier Wall, (Type __; Slab __ in; Wall __ in; Ht __ ft) | LF |
| 608.2013.___ | Concrete, Type I, __ inches thick, Broom Finish, (median slab, etc.) | SY |
| 608.2013.___ | Concrete, Type II, __ inches thick, Exposed Aggregate Finish, (median slab, etc.) | SY |
| 608.2013.___ | Concrete, Type III, __ inches thick, Colored, (median slab, etc.) | SY |
| 608.2013.___ | Concrete, Type IV, __ inches thick, Pattern Imprinted, (median slab, etc.) | SY |
| 608.2013.___ | Concrete, Type V, __ inches thick, Colored and Pattern Imprinted, (median slab, etc.) | SY |
| 608.2014.___ | Concrete Medians | SY |
| 608.2015.___ | Concrete Stairway | LS |
| 608.2032.___ | Detectable Warning Tile | SY |

CR608-113020R

Pay Items, Numbers, Descriptions, and Units.

•	Fill in the blank with the description (wall type I/II/III, slab/wall thickness, wall height, slab description, etc.). Remove the () and match what you used for the AWP supplemental description.

•	There are other pay items in AWP; however, the pay items listed here are the CR preferred items.