Special Provisions

Replace Section 610 with the following:

SECTION 610
DITCH LINING

610-1.01 DESCRIPTION. Construct ditch lining at the locations on the Plans or as staked.

Sect 610: CR610-060117R. Replaces the SSHC 2020 Section.	Related Sect/Sp: 611.

No mention is made of round stones to their exclusion.  Designer, if your project has significant slopes, that are 3:1 or flatter, you may allow round stones (place-rounded stones on slopes 3:1 or flatter). The use of round stones should be rare and should have the input from the PM, the hydrology and construction departments.

610-2.01. MATERIALS. Use crushed stones that are angular, hard, sound, and durable with at least one face resulting from fracture.

1.	Angular—stones, the particles of which possess well-defined edges formed at the intersection of roughly planar faces.

2.	Hardness—resistance of a material to indentation or scratching. AASHTO T96, not more than 50% wear at 500 revolutions.

3.	Soundness—measure of aggregates durability when exposed to the elements, AASHTO T104.

4.	Gradation—ATM 304:

a.	Maximum of 6 inches in greatest dimension

b.	Not more than 50% by weight passing a 3-inch sieve

c.	Not more than 5% passing a 1-inch sieve

5.	Breadth and Width—at least 1/3 of the length

610-3.01 CONSTRUCTION REQUIREMENTS. Place and spread ditch lining materials so that the finished face is uniform. 	Place stones on slopes 1.5:1 and flatter.

610-4.01 METHOD OF MEASUREMENT. Section 109.

610-5.01 BASIS OF PAYMENT. Excavation required below normal ditch grade is subsidiary.

| pay item |  |  |
| --- | --- | --- |
| Item Number | Item Description | Unit |
| 610.0001.____ | Ditch Lining | CY |
| 610.0002.____ | Ditch Lining | Ton |
| 610.0003.____ | Ditch Lining | STA |

CR610-060117R