section 632

paving fabric

Special Provisions

Sect 632: C632.1	Related Sect/Sp: 619, 630, 631, 633, 634, 641, 727, 729

Apply to project

632-3.01 CONSTRUCTION.

2.	Application of Sealant.

Replace the 2nd Sentence with:

Apply the asphalt sealant uniformly at 0.20 to 0.30 gallons per square yard and at a temperature of between 295 F min. and 320 F max. in the distributor tank, or as directed by the Engineer and/or Paving Fabric manufacturer.

4.	Fabric Placement.

Add the following:

Do not allow the Geotextile to become wet.

C632.1-20.0101