SECTION 702
ASPHALT MATERIALS

Standard Modification

Section 702: C702.3 replaced by HSM20.44	Related Sect/Sp: 306/C306, 401/C401, 408/C408

Apply to all projects with work related to Section 702

Replace Subsection 702-2.01 with the following:

702-2.01 ASPHALT BINDER. Meet AASHTO M 320 or M 332 for the specified Performance Grade, except as indicated in Table 702-2.01-1 Exceptions to Performance-Graded Binder Specifications.

TABLE 702-2.01-1

EXCEPTIONS TO PERFORMANCE GRADED ASPHALT BINDER SPECIFICATIONS

| Performance Grade | AASHTO Specification | Viscosity AASHTO T 316 | MSCR, AASHTO T 350 |  |  | PAV, Dynamic Shear AASHTO T 315 | Direct Tension AASHTO T 314 |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | JNR3.2 kPa-1 | JNR Diff | % Recovery3.2 |  |  |
| PG 52-28 | M 320 | None |  |  |  | None | Delete |
| PG 52-34 E | M 332 | None | None | Delete | 60 min. | None | Delete |
| PG 58-28 E | M 332 | None | None | Delete | 60 min. | None | Delete |
| PG 58-34 V | M 332 | None | None | Delete | 60 min. | None | Delete |
| PG 64-28 E | M332 | None | None | Delete | 60 min. | None | Delete |
| PG 52-40 E | M 332 | None | None | Delete | 75 min. | None | Delete |
| PG 58-34 E | M 332 | None | 0.25 max. | Delete | 85 min. | None | Delete |
| PG 64-40 E | M 332 | 1 Pas max. | 0.10 max. | Delete | 95 min. | 5000 max. @ 4°C | Delete |

None indicates no exceptions from the listed test. Delete indicates this property is not required from the listed test.

Use asphalt binders without re-refined engine oil bottoms (REOB)/vacuum tower extenders (VTAE) as a modifier. REOB/VTAE are materials as defined in the Asphalt Institute document IS-235. Furnish a certificate of compliance according to Subsection 106-1.05.1 certifying that REOB/VTAE were not used as a modifier of asphalt binder.

702-2.07 WARM MIX ASPHALT (WMA). Add the following to Table 702-3:

| WMA Technology | Process Types | WMA Supplier |
| --- | --- | --- |
| AD-here ULTRA 1 | Chemical Additive | Arkema – Road Science |
| Cecabase RT | Chemical Additive | Arkema – Road Science |

HSM20.44-23.0801