Section 703

SECTION 703
AGGREGATES

Special Provision
703-2.07 SELECTED MATERIAL.

Replace 1. Type A with the following:

1.
Type A. Aggregate containing no muck, frozen material, roots, sod or other deleterious matter and with a plasticity index not greater than 6 as tested by ATM 204 and ATM 205.  Meet the following gradation as tested by ATM 304:

Sieve
Percent Passing by Weight
No. 4
20-55%

No. 200
0-6%, determined on the minus 3-inch portion of the sample

C703.2-26.0215
Section 703: C703.2-22.0501. Separated from C703.1	Related Sect/Sp: 201, 203, 204/C204


	Apply to all projects with work related to Section 703













1
ALASKA YYYY


2
ALASKA YYYY

