Section 703

SECTION 703
AGGREGATES

Special Provision
Replace Subsection 703-2.10 with the following:

703-2.10 POROUS BACKFILL MATERIAL. Gravel consisting of crushed or naturally occurring granular material containing not more than 1.0% clay lumps or other readily decomposed material, AASHTO T 112. Meet the grading requirements of Table 703-10 as determined by ATM 304.
Use Gradation A unless otherwise specified.

	table 703-10

aggregate gradation for porous backfill

	Sieve
	Percent Passing by Weight

	
	Gradation A
	Gradation B
	Gradation C

	3 in.
	100
	--
	--

	2 in.
	--
	100
	--

	1 1/2 in.
	--
	95-100
	--

	1 in.
	0-10
	--
	100

	3/4 in.
	--
	0-20
	0-20

	3/8 in.
	-
	0-5
	0-5

	No. 200
	0-5
	0-2
	0-2


C703.3-26.0215
Section 703: C703.3-26.0215	Related Sect/Sp:  204/C204, 205, 511/C511


	Apply to all projects with work related to Section 703













1
ALASKA YYYY


2
ALASKA YYYY

