Section 703

SECTION 703
AGGREGATES

Special Provision
Replace Subsection 703-2.13 with the following:
703-2.13 STRUCTURAL FILL. Aggregate containing no muck, frozen material, roots, sod or other deleterious matter and with a plasticity index not greater than 6 as determined by ATM 204 and ATM 205. Meet the grading requirements of Table 703-12 as determined by ATM 304.
	TABLE 703-12

AGGREGATE GRADATION FOR STRUCTURAL FILL

	Sieve
	Percent Passing by Weight

	3-inch
	100

	3/4-inch
	75-100

	No. 4
	20-55

	No. 200
	0-6


C703.4-26.0215
Section 703: C703.4-26.0215. C703.4 separated from C703.1.	Related Sect/Sp:204/C204, 205, 511/C511


	Apply to all projects with work related to Section 703













1
ALASKA YYYY


2
ALASKA YYYY

