Section 703

SECTION 703
AGGREGATES

Special provision
Add the following Subsection 703-2.17 Bedding Material:

703-2.17 BEDDING MATERIAL. Aggregate containing no muck, frozen material, roots, sod, or other deleterious matter and with a plasticity index not greater than 6 as tested by ATM 204 and ATM 205. Meet the following gradation as tested by ATM 304:

	table 703-2.17-1

aggregate gradation for bedding material

	Sieve
	Percent Passing by Weight

	
	Gradation A
	Gradation B

	1 in.
	100
	--

	1/2 in.
	--
	100

	No. 4
	20-75
	20-75

	No. 200
	0-6
	0-6


C703.6-26.0215

Section 703: C703.6-26.0215	Related Sect/Sp: 201/C201.1.2; 204/C204


	Apply to all projects with work related to Section 703













1
ALASKA YYYY


2
ALASKA YYYY

