Section 703

SECTION 703
AGGREGATES

Special Provision
703-2.03 AGGREGATE FOR BASE AND SURFACE COURSE.
In Table 703-1 replace the line for Degradation Value with the following:

	table 703-1

aggregate quality properties for base and surface course

	Description
	Specification
	Base Course
	Surface Course

	Micro-Deval, % max.
	AASHTO T 327
	15
	15


C703.7-26.0215
703-2.05 AGGREGATE FOR COVER COAT AND SURFACE TREATMENT.
In Table 703-5 replace the line for Degradation Value with the following:

	TABLE 703-5
QUALITY PROPERTIES FOR COVER COAT AND SURFACE TREATMENT

	Description
	Specification
	Aggregate

	Micro-Deval, % max.
	AASHTO T 327
	15


C703.7-26.0215
703-2.09 SUBBASE. 

In Table 703-8 replace the line for Degradation Value with the following:

	TABLE 703-8

QUALITY PROPERTIES FOR SUBBASE

	Description
	Specification
	Subbase

	Micro-Deval, % max.
	AASHTO T 327
	25


C703.7-26.0215
Section 703: C703.7. HSM20.40 included in C703.1 and C703.7	Related Sect/Sp: 201/C201.1.2; 204/C204,306/C306, 401/C401, 408/C408


	Apply to all projects with work related to Section 703	













1
ALASKA YYYY


2
ALASKA YYYY

