SECTION 703
AGGREGATES

Standard Modification

Section 703: HSM20.40-22.0501. Table 703-3 C703.1 incorporated HSM20.40	Related Sect/Sp: 201/C201.1.2; 206/C306, 401/C401, 408/C408, 703/C703.1

Apply to all projects with work related to Section 703

703-2.03 AGGREGATE FOR BASE AND SURFACE COURSE.

In Table 703-1 replace the line for Degradation Value with the following:

TABLE 703-1

AGGREGATE QUALITY PROPERTIES FOR BASE AND SURFACE COURSE

| PROPERTY | BASE COURSE | SURFACE COURSE | TEST METHOD |
| --- | --- | --- | --- |
| Micro-Deval | 15%, max. | 15%, max. | AASHTO T 327 |

HSM20.40-22.0501

Special Provision

703-2.04 AGGREGATE FOR HOT MIX ASPHALT.

HSM20.40 Table 703-3 is incorporated into C703.1

In Table 703-3 replace the line for Degradation Value with the following:

TABLE 703-3

COARSE AGGREGATE QUALITY FOR HMA

| Description | Specification | Type II, Class A | Type I; Type II, Class B; Type III | Type IV | Type VH |
| --- | --- | --- | --- | --- | --- |
| Micro-Deval, % max. | AASHTO T 327 | 18 | 18 | 18 | 18 |

C703.1-22.0501

703-2.05 AGGREGATE FOR COVER COAT AND SURFACE TREATMENT.

In Table 703-5 replace the line for Degradation Value with the following:

TABLE 703-5

QUALITY PROPERTIES FOR COVER COAT AND SURFACE TREATMENT

| Micro-Deval | AASHTO T 327 | 15%, max. |
| --- | --- | --- |

703-2.09 SUBBASE.

In Table 703-8 replace the line for Degradation Value with the following:

TABLE 703-8

QUALITY PROPERTIES FOR SUBBASE

| Micro-Deval | AASHTO T 327 | 25%, max. |
| --- | --- | --- |

HSM20.40-22.0501