Section 710

SECTION 710
FENCE AND GUARDRAIL
Special Provision
Replace Subsection 710-2.04 with the following:
710-2.04 METAL BEAM RAIL.
1.
W-Beam and Thrie Beam Guardrail. Meet AASHTO M 180, Class A, Type II.

2.
Box-Beam Guardrail. Meet ASTM A500 Grade B, or ASTM A501.
3.
Symmetric and Asymmetric W-Thrie Beam Transition Section. Meet AASHTO M 180, Class B, 
Type II.

Galvanize the rail per AASHTO M 111 after fabrication.

710-2.06 GUARDRAIL POSTS AND BLOCKOUTS.
Add the following:

4.
Transition Posts. Meet the section and length specified on the Plans. Meet ASTM A992 or ASTM A709, Grade 50.

5.
Transition Blockouts. Meet the shape and dimensions shown on the Plans. Meet ASTM A500. Grade B or Grade C.
Add the following Subsection 710-2.12 Transition Connection:
710-2.12 TRANSITION CONNECTION.
1.
Thrie Beam Terminal Connector. Meet AASHTO M 180, Class B, Type II.

2.
Guardrail Connection Plate. Meet ASTM A709, Grade 50.

C710.4-25.1105
Section 710: C710.4-25.1105	Apply to all projects with work related to Section 710	Related Sect/Sp: 606/C606/C606.9.10.13.


HSM20.34-21.1231 replaced by:    C710.4-25.1105:  710-2.04, 2.06, 2.12     &    HSP20.12-25.1105:  710-2.11 













1
ALASKA YYYY


2
ALASKA YYYY

