Section 710

SECTION 710
FENCE AND GUARDRAIL
Special Provision
Replace Subsection 710-2.04 with the following:
710-2.04 METAL BEAM RAIL.
1.
W-Beam and Thrie Beam Guardrail. Meet AASHTO M 180, Class A, Type II.

2.
Box-Beam Guardrail. Meet ASTM A500 Grade B, or ASTM A501.
3.
Symmetric and Asymmetric W-Thrie Beam Transition Section. Meet AASHTO M 180, Class B, 
Type II.

Galvanize the rail per AASHTO M 111 after fabrication.

710-2.06 GUARDRAIL POSTS AND BLOCKOUTS.
Add the following:

4.
Transition Posts. Meet the section and length specified on the Plans. Meet ASTM A992 or ASTM A709, Grade 50.

5.
Transition Blockouts. Meet the shape and dimensions shown on the Plans. Meet ASTM A500. Grade B or Grade C.
C710.4-25.1105

Replace Subsection 710-2.11 with the following:
710-2.11 GUARDRAIL TERMINALS.

W-beam shall meet requirements of AASHTO M 180, Class A, Type II. Box beam shall meet requirements of ASTM A500 Grade B, or ASTM A501. Galvanize after fabrication.

Components made from rolled pressed and forged shapes, castings, plates, bars, and strips shall meet the coating requirements of AASHTO M 111. Galvanize after fabrication.

All hardware or fasteners supplied shall meet the coating requirements of AASHTO M 232.

Guardrail Terminals shall be AASHTO MASH Test Level 3.

1.
W-Beam. Provide one of the following terminal types, as shown on the plans, for single-rail W-beam guardrail. Design requirements: 31-inch top of rail height, 8-inch blockouts, W6x8.5 steel posts, 12 ft 6-inch w-beam panels, and mid-span splice connection to run of rail.

a.
Parallel Terminals. Provide the RoadSystems, Inc. MASH MSKT W-Beam terminal with the following characteristics:

(1)
Length: 50 ft nominal effective length.

(2)
End Offset: 0 ft to 2 ft (25:1 or flatter straight taper). Offset end as shown on the plans.

b.
Buried in Backslope Terminal. Provide terminals as shown on the Plans.

2.
Box Beam. Provide terminals, as shown on the plans for box beam guardrail. Design requirements: 28-inch top of rail height, designed for use with 6-inch x 6-inch x 3/16-inch box beam.

a.
Parallel Terminals. Provide terminals meeting the following:

(1)
Length: 33 ft nominal effective length, or a minimum 18 ft of box beam rail and standard 3-inch weak posts beyond the 1/8-inch tube rail, or as recommended by the manufacturer's installation manual.

(2)
End Offset: 25:1 or flatter straight taper. Offset end as shown on the plans.
HSP20.12-25.1105

Add the following Subsection 710-2.12 Transition Connection:
710-2.12 TRANSITION CONNECTION.
1.
Thrie Beam Terminal Connector. Meet AASHTO M 180, Class B, Type II.

2.
Guardrail Connection Plate. Meet ASTM A709, Grade 50.

C710.4-25.1105
Section 710: C710.4.HSP20.12-25.1105	Apply to all projects with work related to Section 710	Related Sect/Sp: 606/C606/C606.9.10.13.


HSM20.34-21.1231 replaced by:    C710.4-25.1105:  710-2.04, 2.06, 2.12     &    HSP20.12-25.1105:  710-2.11 













1
ALASKA YYYY


2
ALASKA YYYY

