SECTION 712
MISCELLANEOUS

Special Provisions

Section 712: HSM20.35-123121. HSM20.35 replaces HSM20.35.	Related Sect/Sp: 643, 670/CR670.1

Apply to all projects with work related to Section 712

712-2.08 GLASS BEADS.

Replace the 2nd sentence with the following:

Glass beads shall contain no more than 200 ppm of lead or 200 ppm of arsenic when tested in accordance with EPA testing methods 3052, 6020B, or 6020C.

HSM20.35-123121