SECTION 722
BRIDGE RAILING

Standard Modification

Section 722: HSM20.37	Related Sect/Sp: 507

Apply to all projects with work related to Section 722

Replaces Subsection 722-2.01 Bridge Railing with the following:

722-2.01 BRIDGE RAILING.

| Steel tube rail elements | ASTM A500, Grade B or Grade C |
| --- | --- |
| Steel thrie beam rail elements | AASHTO M 180, Class B, Type II |
| Posts | ASTM A709, Grade 50 |
| Machine bolts, cap screws, nuts and washers | ASTM A307 |
| High strength bolts, nuts and washers | Subsection 716-2.03 |
| Anchor bolts and rods | ASTM F3125, Grade A325 or ASTM A449, Type 1 |
| Welded studs | AASHTO M 169, Grade 1015 or 1020 |
| Bent anchor rods | ASTM A709, Grade 36 or Grade 50 |
| Shims, plates, plate washers, angles, sleeves, and scuppers | ASTM A709, Grade 50 |
| Beveled washers and tapered plate washers | ASTM F436 |
| Galvanize steel portions of railing after fabrication. | AASHTO M 111 or M 232 and Subsection 716-2.07 |

HSM20.37-21.1231R