SECTION 722
BRIDGE RAILING

Standard Modification

Section 722: HSM20.37	Related Sect/Sp: 507

Apply to all projects with work related to Section 722

Replaces Subsection 722-2.01 Bridge Railing with the following:

722-2.01 BRIDGE RAILING.

Steel tube rail elements	ASTM A500, Grade B or Grade C

Steel thrie beam rail elements	AASHTO M 180, Class B, Type II

Posts	ASTM A709, Grade 50

Machine bolts, cap screws, nuts and washers	ASTM A307

High strength bolts, nuts and washers	Subsection 716-2.03

Anchor bolts and rods	ASTM F3125, Grade A325 or

ASTM A449, Type 1

Welded studs	AASHTO M 169, Grade 1015 or 1020

Bent anchor rods	ASTM A709, Grade 36 or Grade 50

Shims, plates, plate washers, angles, sleeves, and scuppers	ASTM A709, Grade 50

Beveled washers and tapered plate washers	ASTM F436

Galvanize steel portions of railing after fabrication.	AASHTO M 111 or M 232 and

Subsection 716-2.07

HSM20.37-21.1231-1