SECTION 301

AGGREGATE BASE AND SURFACE COURSE

Special Provisions

301-2.01 MATERIALS.  Add the following after the first sentence:

Recycled Asphalt Material (RAM) may be substituted for aggregate base course, inch for inch, if the following conditions are met:

1.	RAM shall be crushed or processed to 100 percent by weight passing the 1.5 inch sieve and 95-100 percent by weight passing the 1 inch sieve.

2.	The gradation of the extracted aggregate shall meet the following:

| Sieve | Percent Passing by Weight |
| --- | --- |
| 1 inch | 100 |
| 3/4 inch | 70 – 100 |
| 3/8 inch | 42 – 90 |
| No. 4 | 28 – 78 |
| No. 16 | 11 – 54 |
| No. 50 | 5 – 34 |
| No. 100 | 3 - 22 |
| No. 200 | 2 – 12 |

3.	The asphalt content shall be 2.5 – 5.0 percent by weight of the RAM.

CR176-012407

301-3.03 SHAPING AND COMPACTION.  Add the following:

If recycled asphalt material is substituted for aggregate base course, the following conditions shall be met:

1.	Density acceptance will be determined by control strip method ATM 412.  Use a test strip with a vibratory compactor with a minimum dynamic force of 40,000 pounds.  The optimum density will be determined by the Engineer using a nuclear densometer gauge to monitor the test strip.  Adequate water shall be added to aid compaction.

2.	After the appropriate coverage with the vibratory compactor, a minimum of 6 passes with a pneumatic tire roller shall be completed.  Tires shall be inflated to 80 psi ( 5 psi) and the roller shall have a minimum operating weight per tire of 3,000 pounds.

3.	Aggregate base course, or RAM, in areas of shoulder buttressing, approaches, and driveway transitions shall be compacted and approved by the Engineer.  Testing for density is not required.

301-4.01. METHOD OF MEASUREMENT.  Add the following:

Aggregate base course used for shoulder buttressing, approaches, and driveway transitions is incidental to other items.

Aggregate base course is included in the measurement of the following items required as part of the installation, modification and or repair of the items:

- Aggregate base course for shoulder buttressing is measured as part of 401 Items.

- Aggregate base course for approaches and driveways is measured as part of 639 Items.

- Aggregate base course for Highway Spot Repair work is measured as part of 680 Items.

301-5.01 BASIS OF PAYMENT.  Add the following:

Recycled asphalt material substituted for aggregate base course will be paid for as Item 301(1) Aggregate Base Course at the unit price shown in the bid schedule for that item, except that aggregate base course is subsidiary to the following sections and associated items:

- Used for shoulder buttressing – Section 401 Items

- Used for approaches and driveways – Section 639 Items

- Used for Highway Spot Repair work – Section 680 Items

52493-032210