Special Provisions

Replace Section 502 with the following:

SECTION 502

PRESTRESSING CONCRETE

502-1.01 DESCRIPTION. Prestress precast or cast-in-place concrete by furnishing, placing, tensioning, and bonding prestressing steel by using either pretensioning or post-tensioning methods or a combination of the two methods according to the Contract documents.

For pretensioning, this work also includes furnishing and installing all materials and equipment necessary to prestress concrete as designated in the Contract documents.

For post-tensioning, this work includes furnishing and installing all post-tensioning systems and all other pertinent items necessary for the particular prestressing system used, including but not limited to ducts, anchorage assemblies, supplementary reinforcement, and grout used for pressure grouting ducts.

502-1.02 DEFINITIONS.

ANCHORAGE. An assembly of various hardware components that secure a tendon at its ends after it has been stressed imparting the tendon force into the concrete.

ANTICIPATED SET. The set that was assumed to occur in the design calculation of the post-tensioning forces immediately after load transfer.

BEARING PLATE. Hardware that transfers the tendon force directly into concrete.

BLEED. The autogenous flow of mixing water within or its emergence from newly placed grout caused by the settlement of the solid materials within the mass and filtering action of strands.

DUCT. Material forming a conduit to accommodate prestressing steel installation and provide an annular space for the grout that protects the prestressing steel.

FLUIDITY. A measure of time, expressed in seconds, necessary for a stated quantity of grout to pass through the orifice of a flow cone.

GROUT. A mixture of cementitious materials and water with or without mineral additives or admixtures proportioned to produce a pumpable consistency without segregation of the constituents when injected into the duct to fill the space around the prestressing steel.

GROUT CAP. A device that contains the grout and forms a protective cover sealing the post-tensioning steel at the anchorage.

POST-TENSIONING. A method of prestressing in which the tendons are tensioned after the concrete has reached a specified strength.

PRESTRESSING STEEL. The steel element of a post-tensioning tendon, which is elongated and anchored to provide the necessary permanent prestressing force.

POST-TENSIONING SCHEME OR LAYOUT. The pattern, size and locations of post-tensioning tendons.

POST-TENSIONING SYSTEM. An assembly of proprietary post-tensioning hardware, including but not limited to anchorage assembly, local zone reinforcement, wedge plate, wedges, bearing plate, prestressing steel, duct, duct connections, vents and grout cap, used to construct a tendon of a particular size and type.

SET (Also Anchor Set or Wedge Set). The total movement of a point on the strand outside the anchoring wedges during load transfer from the jack to the permanent anchorages. Set movement is the sum of slippage of the wedges with respect to the anchorage head and the elastic deformation of the anchor components.

STRAND. An assembly of several high-strength steel wires wound together. Strands usually have six outer wires helically wound around a single straight wire of a similar diameter.

STRAND COUPLER. An assembly by which the prestressing force may be transmitted from one partial length prestressing tendon to another. (Strand couplers are not permitted.)

TENDON. A single or group of prestressing steel elements and their anchorage assemblies that imparts prestress to a structural member. Also, included are ducts, grouting attachments, grout and corrosion protection filler materials or coatings.

TENDON SIZE. The number of individual strands of a certain strand diameter.

THIXOTROPIC. The material property exhibited by certain grouts that enable material to stiffen, achieve a higher viscosity, in a short time while at rest, but to become liquid, acquire a lower viscosity, when mechanically agitated.

VENT. Tubing or pipe used for injection of grout into the duct and to allow escape of air, water, grout and bleed water from the duct.

WEDGE. A conically shaped device that anchors the strand in the wedge plate.

WEDGE PLATE. The hardware that holds the wedges of a multi-strand tendon and transfers the tendon force to the anchorage assembly.

502-2.01 MATERIALS. Use materials that conform to the following:

Concrete	Section 501

Water	Subsection 712-2.01

Reinforcing steel 	Subsection 709-2.01

Epoxy-Coated Reinforcing Steel	Subsection 709-2.01

Prestressing Steel and Fittings	Section 721

Post-tension Grout	Subsection 701-2.08

Zinc-Rich Paint	Subsection 708-2.01.1

Epoxy Bonding Agents	AASHTO M 235, Type V

CONSTRUCTION REQUIREMENTS

502-3.01 PRETENSIONING METHODS. Select a pretensioning method that provides the magnitude and distribution of prestressing force specified in the Contract documents, subject to the requirements in this Section and approval by the Engineer.

1.	Shop Drawings. Before casting members to be prestressed, submit for approval shop drawings including complete details and substantiating calculations of the method, materials, and equipment proposed for use in the prestressing operations, any additions or rearrangement of reinforcing steel, and any revision in concrete dimensions.

Include an outline of the method and sequence of stressing, complete specifications and details of the prestressing steel and anchoring devices to be used, anchoring stresses, strand release sequence, and other data pertaining to the prestressing operations, including the proposed arrangement of the prestressing units in the members.

Compute the anticipated camber at the time of prestressing force transfer and at other significant times. Show the values on the shop drawings as a time/deflection curve, subject to approval.

Include on shop drawings embedded items such as reinforcing steel, lifting devices, coil anchors, anchor bolts, drainage systems, utility conduits and other such items. Ensure there will be no conflict between the planned positions of any embedded items and that concrete cover will be adequate.

2.	Quality Control Plan. Submit for approval a quality control plan that verifies that all materials and workmanship incorporated into the prestressed concrete members conform to the requirements.

Perform all pretensioning operations under the direct supervision and control of a qualified pretensioning technician. Provide a pretensioning technician, skilled in the prestressing method, to aid and instruct in using the prestressing equipment and in installing the materials to obtain required results.

3.	Protection of Prestressing Steel. Protect prestressing steel and anchor assemblies against physical damage and corrosion at all times. Keep prestressing steel and anchor assemblies clean and free of deleterious material such as grease, oil, wax, paint, or other foreign materials. The Engineer will reject prestressing steel that has at any time sustained physical damage. The Engineer will reject prestressing steel that has developed visible rust pitting or other results of corrosion, other than rust stain.

Protect prestressing steel and anchorage assemblies against physical damage and corrosion during shipping and storage by packaging the prestressing steel and anchorage assemblies in containers or shipping forms. Place a corrosion inhibitor in the package or form, incorporate a corrosion inhibitor carrier-type packaging material, or apply a corrosion inhibitor directly to the steel. Do not use corrosion inhibitors that have deleterious effect on the steel or concrete or bond strength of steel to concrete. Immediately replace packaging or forms damaged from any cause or restore packaging to original condition.

Clearly mark the shipping package or form with a statement that the package contains high-strength prestressing steel, and the type of corrosion inhibitor used, including the date packaged.

4.	Prestressing Equipment. Use hydraulic jacks to tension prestressing steel strands so that the force in the prestressing steel will not be less than the value specified in the Contract documents or as approved by the Engineer.

Equip each jack used to stress strands with either:

a.	two pressure gages

b.	one pressure gage and one load cell

In the event that any uncertainty exists regarding jack calibration, pressure gage usage, strand elongation or any other prestressing strand tensioning issue, provide and use a calibrated load cell when prestressing steel strands.

Permanently mark the jack body with the ram area. Ensure each pressure gage is fully functional, calibrated and has an accurately reading dial at least 6 inches in diameter.

Calibrate the jack and each gage, used to stress strands, as a unit within 6 months prior to use and after each repair. If used, provide a load cell calibrated within the past 12 months with an indicator that may be used to determine the prestressing force in the strand. The range of the load cell shall be such that the lower 10 percent of the manufacturer's rated capacity will not be used in determining the jacking stress.

Use the following calibration procedure; Perform three calibration test cycles with the cylinder extension of the jack in various positions (i.e. 2 inch, 4 inch, 8 inch stroke). At each pressure increment, average the forces from each test cycle to obtain an average force. Perform the calibration with the equipment setup in the same configuration that will be used at the job site. Use load cells calibrated within the past 12 months to calibrate stressing equipment.

For each jack and gauge unit used on the project, provide the Engineer with certified calibration curves prior to the start of the work and every 6 months thereafter, or as requested by the Engineer. If used, supply documentation denoting the load cell calibration date prior to the start of the work and every 6 months thereafter. Furnish certified calibration charts to the Engineer prior to stressing.

Recalibrate jacks requiring repair, such as replacing seals or changing the length of the hydraulic lines. No extra compensation will be allowed for the initial or subsequent calibrations.

5.	Placing Reinforcing Steel and Prestressing Steel. Place reinforcing steel according to Section 503, except as modified by this section.

Place prestressing steel in the position as designated in the Contract documents or on the approved shop drawings.

6.	Girder Inserts. Provide threaded inserts, coil anchors, or approved equal in the girder as indicated in the Contract documents.

With the written approval of the Engineer, additional inserts in the girder may be provided to accommodate diaphragm forms or other construction related requirements.

Provide holes in the girder web as indicated on the plans to accommodate reinforcing steel. Verify that the hole size is sufficient to accommodate reinforcement placement procedures.

7.	Pretensioning. Stress strands to the magnitude specified in the Contract documents by either single strand stressing or multiple strand stressing. Prior to applying full pretensioning, bring all strands to be stressed in a group (multiple strand stressing) to a uniform initial tension that is sufficient to eliminate all slack and equalize the stresses in the strands. Limit the strand stress in pretensioned members before seating (jacking stress) to 70 percent of the minimum breaking strength (0.70 fpu) of the prestressing steel.

Ensure that the tension load indicated by the gauge(s) is within 5 percent of the calculated tension load based on elongation measurements for each strand.

Use approved low-friction devices at all points of change in slope of strand trajectory when tensioning harped strands.

Tension harped strands from both ends of the bed if the prestressing force, as determined by elongation measurements, is less than 95 percent of that indicated by the jack gauges. Ensure the computed load from the sum of elongation at both ends is within 5 percent of that indicated by the jack gauges.

When splicing strands, locate all splices outside of the prestressed units. Account for additional elongation due to the splice when verifying the tension load based on elongation measurements.

Keep the temperature of the strands during tensioning and concrete placement within 25°F of the concrete temperature during placement. During the interval between tensioning and concrete placement, do not let temperature changes alter the stress level in the strands more than 5 percent of the jacking stress, nor cause the stress in the strand to exceed 75 percent of the minimum breaking strength.

8.	Placing Concrete. Produce and place concrete according to the requirements of Section 501, except as modified by this section.

Before depositing concrete in the forms, obtain an inspection of the reinforcing steel, enclosures, anchorages, and prestressing steel by an authorized Department representative.

Consolidate the concrete using any combination of internal and external vibration that does not displace the reinforcing steel or other items embedded in the concrete.

9.	Release. Do not release prestressing strands or transfer prestressing forces to the member until concrete cylinder tests, manufactured according to AASHTO T 23 and tested according to AASHTO T 22 using the same concrete and maintained in the same curing conditions as the member, indicate that the concrete has attained the minimum initial compressive strength (release strength, f'ci) as indicated in the Contract documents.

Cut or release the elements in an order that minimizes the lateral eccentricity of the pre-stress. Cut all prestressing strands to a depth of at least 1 inch from the concrete surface. Fill the recess with cement mortar and finish flush to the concrete surface. Alternatively, cut all prestressing strands flush with the end of the member. Clean and paint the exposed ends of the strand and a 1-inch strip of adjoining concrete. Use a wire brush or abrasive blast cleaning to remove all dirt and residue not firmly bonded to the metal or concrete surfaces. Cover the surfaces with a thick application of zinc-rich paint.  Thoroughly mix the paint at the time of application and work it into any voids in the strands. Apply two applications to surfaces that are not covered by concrete or mortar.

502-3.02 POST-TENSIONING METHODS. Select a post-tensioning system that provides the magnitude and distribution of prestressing force specified in the Contract documents, subject to the requirements in this Section and approval by the Engineer.

For box girders, distribute the prestressing steel so that the force in each girder stem does not vary more than 5 percent from the required force per girder stem provided the required total force in the superstructure is obtained and the force is distributed symmetrically about the centerline of the typical section.

Do not exceed 75 percent of the minimum breaking strength of the prestressing steel for maximum temporary tensile stresses (jacking stresses) in prestressing steel. Do not exceed 70 percent of the minimum breaking strength of the prestressing steel at anchorages after anchor set.

Working force and working stress will be considered as the force and stress remaining in the prestressing steel after all losses (e.g., creep and shrinkage of concrete, elastic compression of concrete, creep of steel, losses in post-tensioned prestressing steel due to sequence of stressing, friction and take up of anchorages and all other losses peculiar to the method or system of prestressing) have taken place or have been accommodated. Calculate loss of prestress using industry recognized methods. The calculation and analysis methods are subject to approval by the Engineer.

1.	Shop Drawings and Calculations. Before casting members to be prestressed, submit shop drawings and supporting calculations of the prestressing system to the Engineer for approval no less than 45 days prior to the placement of bridge concrete. Submit four sets of the drawings for initial review. After the initial review has been reviewed and all comments from the Engineer have been received and implemented, submit drawings to the Engineer for approval and for use during construction according to Subsection 105-1.02.

Show complete details on the shop drawings of the prestressing system and all substantiating calculations of the method, materials, and equipment to be used in the prestressing operations, including any additions or rearrangement of reinforcing steel and any revision in concrete dimensions from that shown on the Plans. Outline in sufficient detail the method and sequence of stressing. Include complete specifications and details of the prestressing steel and anchoring assemblies, working stresses, anchoring stresses, type of ducts, initial prestress losses, final prestress losses and all other data pertaining to the prestressing operation. Show tendon geometry and locations complying with the plans and the limitations of the selected post-tensioning system. Show all vent locations, high point outlet inspection details, anchorage inspection details and grout caps, protection system materials and application limits. Include on the shop drawing the location of the anchorages, vents, and duct enclosures at 2-foot (maximum) intervals along the length of the girder.

Submit calculations for the anticipated camber at the time of prestressing force transfer and at other significant times. Show the values on the shop drawings as a time/deflection curve.

Submit calculations for the anticipated tendon elongation. Utilize the modulus of elasticity, based on nominal area, as furnished by the prestressing steel manufacturer for the lot of steel being tensioned. Show a typical tendon force diagram, after friction, wobble and anchor set losses, on the shop drawings based upon the expected friction curvature and wobble coefficients and values for the post-tensioning system used. Show the coefficients and values on the shop drawings.

Produce all shop drawings related to post-tensioning by a Professional Engineer specializing in post-tensioning concrete. Bear the signature and seal of the Professional Engineer who specializes in post-tensioning construction on all calculations, drawings, and procedures.

Include post-tensioning system certification(s) conforming to Subsection 721-2.04.

2.	Post-tensioning Technician. Perform all post-tensioning field operations under the direct supervision of a qualified post-tensioning technician. Provide a post-tensioning technician with at least five years of experience in construction of post-tensioned prestressed concrete structures. Provide a technician, skilled in the prestressing method, to aid and instruct in using the prestressing equipment and in installing the materials to obtain required results.

Perform all grouting under the direct supervision of a certified grouting technician. Provide a technician skilled in various aspects of grouting whom the American Segmental Bridge Institute certifies as an "ASBI Certified Grouting Technician".

The post-tensioning technician shall be present at all times during duct installation, tendon tensioning, and grouting operations and shall provide close observation and control of all post-tensioning and grouting operations, as necessary for compliance with the Contract. Submit the name of the post-tensioning technician and proof of certification to the Engineer no less than thirty days before the start of bridge concrete placement operations.

Do not substitute post-tensioning technicians without prior written approval from the Engineer. Provide documentation demonstrating that the proposed substitute individual meets the qualifications. All post-tensioning operations will be suspended if the Engineer has not approved the proposed substitution in writing. If work is delayed or suspended due to unapproved substitutions of special qualification personnel, no additional Contract time or additional compensation will be allowed according to Subsection 108-1.06.

3.	Protection of Prestressing Steel and Anchorages. Protect prestressing steel and anchor assemblies against physical damage and corrosion at all times from manufacture to grouting. Keep prestressing steel and anchor assemblies clean and free of deleterious material such as grease, oil, wax, paint, or other foreign materials. The Engineer will reject prestressing steel that has at any time sustained physical damage. The Engineer will reject prestressing steel that has developed visible rust pitting or other results of corrosion, other than rust stain.

Protect prestressing steel and anchorage assemblies against physical damage and corrosion during shipping and storage by packaging the prestressing steel and anchorage assemblies in containers or shipping forms. Place a corrosion inhibitor in the package or form, incorporate a corrosion inhibitor carrier-type packaging material, or apply a corrosion inhibitor directly to the steel. Do not use corrosion inhibitors that have deleterious effect on the steel or concrete or bond strength of steel to concrete. Immediately replace packaging or forms damaged from any cause or restore packaging to original condition.

Clearly mark the shipping package or form with a statement that the package contains high-strength prestressing steel, and the type of corrosion inhibitor used, including the date packaged.

If prestressing steel is installed in ducts but not tensioned and grouted within the seven days, perform Nondestructive Examination (NDE) by either videoscoping the entire length of the prestressing steel inside the ducts or visually inspecting the prestressing steel upon removing the prestressing steel from the duct for corrosion. Perform NDE inspection at least once every seven days until the prestressing steel is tensioned and grouted. Perform NDE inspection to the satisfaction of the Engineer. Provide a report of the tendon condition to the Engineer following each NDE inspection for each tendon installation.

If corrosion is not found on the prestressing steel upon completion of NDE inspection, the Engineer may require protecting prestressing steel corrosion by means of a corrosion inhibitor placed in the ducts. Do not place a corrosion inhibitor inside the duct if prestressing steel installation, tensioning, and grouting is performed within seven days. Do not use corrosion inhibitors that have deleterious effect on the steel or concrete or bond strength of steel to concrete. Submit for approval the name, manufacturer, and type of corrosion inhibitor to be used in the ducts at least seven days before installation of any prestressing steel. Prior to grouting, flush the corrosion inhibitor from the ducts using a solution of quick lime (calcium oxide) or slaked lime (calcium hydroxide) in the amount of 0.1 lbs/gal. Use compressed air that is oil free to blow out ducts and remove flush water.

Cover and protect the anchorages against corrosion at all times from installation of the prestressing steel to placement of the concrete pour-backs.

Do not weld on or near prestressing steel, ducts, anchorages, or other assemblages. Protect prestressing steel and hardware from weld spatter or other damage. Once the prestressing steel has been installed, do not make welds or grounds for welders on the forms, reinforcing steel, or adjacent steel members.

4.	Prestressing Equipment. Use hydraulic jacks to tension prestressing steel tendons so that the force in the prestressing steel will not be less than the value specified in the Contract documents or as approved by the Engineer. Do not use monostrand jacks to stress multi-strand tendons.

Equip each jack used to stress tendons with either:

a.	two pressure gages

b.	one pressure gage and one load cell

In the event that any uncertainty exists regarding jack calibration, pressure gage usage, strand elongation or any other prestressing strand tensioning issue, provide and use a calibrated load cell when prestressing steel tendons.

Permanently mark the jack body with the ram area. Ensure each pressure gage is fully functional, calibrated and has an accurately reading dial at least 6 inches in diameter.

Calibrate the jack and each gage used to stress tendons as a unit within 6 months prior to use and after each repair. If used, provide a load cell calibrated within the past 12 months with an indicator that may be used to determine the prestressing force in the tendon. The range of the load cell shall be such that the lower 10 percent of the manufacturer's rated capacity will not be used in determining the jacking stress.

Use the following calibration procedure; Perform three calibration test cycles with the cylinder extension of the jack in various positions (i.e. 2 inch, 4 inch, 8 inch stroke). At each pressure increment, average the forces from each test cycle to obtain an average force. Perform the calibration with the equipment setup in the same configuration that will be used at the job site. Use load cells calibrated within the past 12 months to calibrate stressing equipment.

For each jack and gauge unit used on the project, provide the Engineer with certified calibration curves prior to the start of the work and every 6 months thereafter, or as requested by the Engineer. If used, supply documentation denoting the load cell calibration date prior to the start of the work and every 6 months thereafter. Furnish certified calibration charts to the Engineer prior to stressing.

Recalibrate jacks requiring repair, such as replacing seals or changing the length of the hydraulic lines. No extra compensation will be allowed for the initial or subsequent calibrations.

5.	Enclosures for Post-Tensioning. Accurately place enclosures (anchorages, ducts, and vents) for prestressing reinforcing according to the Plans or approved shop drawings.

Set and hold the anchorage assemblies and block-out templates for anchorages so that their axis coincides with the axis of the tendon and the wedge plates are normal in all directions to the tendon. Securely fasten anchorages and block-outs to prevent displacement during concrete placement. Unless otherwise specified in the Contract documents or shown on the approved shop drawings, recess the anchoring assemblies in formed block-outs so that the ends of the prestressing steel and all parts of the anchoring assemblies will be at least 3 inches inside of the end surface of the member. Construct all block-outs in leak proof forms that create neat lines with the end surface of the member.

Securely fasten ducts at the proper locations in the forms by ties to reinforcing steel that are adequate to prevent displacement during concrete placement. Use supplementary support bars where needed to maintain proper alignment of the duct. Use hold-down ties to prevent displacement due to duct buoyancy in the fluid concrete. Fasten ducts at 2-foot maximum intervals along the member.

Do not damage the ducts during installation. Do not crimp, flatten, or dent the ducts. Do not perforate the ducts or provide openings in the ducts except at locations designated in the Contract documents or shop drawings. After duct installation, inspect all ducts for damage. The Engineer will reject ducts with unintentional holes or openings and ducts that are dented, crimped, or flattened. Repair duct sections to the satisfaction of the Engineer at no additional cost to the Department and no adjustment in Contract time.

After installation in the forms, cover the ends of the ducts and anchorages at all times to prevent the entry of water or debris.

Prior to placing forms for closing slabs of box girder cells, demonstrate to the satisfaction of the Engineer that all ducts are unobstructed.

6.	Location of Grout Vents. Place grout vents at locations designated in the Contract documents and shop drawings. Equip all grout vents with positive shut-off devices. Extend grout tubes with sufficient distance out of the concrete member to allow for proper closing of the valves.

7.	Placing Reinforcing Steel and Prestressing Steel. Place reinforcing steel according to the requirements of Section 503 and as modified by this Section.

Place prestressing steel in the position as designated in the Contract documents or on the approved shop drawings. Install the prestressing steel in the enclosures by pushing or pulling the total number of strands in a tendon individually or as a unit.

For strands that are pushed, round off the end of the strand and fit the end of the strand with a smooth protective cap.

For strands that are pulled, use a special steel wire sock or other device attached to the end strands to pull the assembled tendon through the duct. Do not weld the ends of the strands together for this purpose. Round the end of the pre-assembled tendon for smooth passage through the duct. Cut strands using an abrasive saw or equal. Do not flame cut strands.

Immediately prior to installing the prestressing steel, demonstrate to the satisfaction of the Engineer that the ducts are free of water, debris, and other obstructions by passing a torpedo through the ducts. Use a torpedo having the same cross-sectional shape as the duct and is 1/4 inch smaller all around than the clear, nominal inside dimensions of the duct. Make no deductions to the torpedo section dimensions for tolerances allowed in the manufacture or fixing of the ducts. For straight ducts, use a torpedo at least 2 feet long. For curved ducts, determine the length so that when both ends touch the outermost wall of the duct, the torpedo is 1/4 inch clear of the innermost wall. If the torpedo will not travel completely through the duct, the Engineer will reject the member, unless a workable repair can be made to clear the duct. The torpedo must pass through the duct easily, by hand, without resorting to excessive effort or mechanical assistance.

If the strands do not easily pass through the duct or an obstruction is encountered, do not force strands through the duct.

Do not install the prestressing steel in the duct prior to placing and curing of the concrete.

Straighten prestressing steel strands that are to be stressed simultaneously or when necessary to ensure proper positioning in the ducts.

8.	Placing Concrete. Produce and place concrete according to the requirements of Section 501 and as modified by this section.

Before depositing concrete in the forms, obtain an inspection and approval of the placement of reinforcing, enclosures, anchorages, and prestressing steel. Vibrate the concrete internally, externally, or both, as directed by the Engineer. Vibrate carefully to avoid displacing the reinforcing steel, anchorages, ducts, grout vents, or other items embedded in the concrete.

9.	Post-tensioning. Do not begin tensioning operations until concrete cylinder tests, manufactured according to AASHTO T 23 and tested according to AASHTO T 22 using the same concrete and maintained in the same curing conditions as the member, indicate that the concrete has attained the minimum initial compressive strength (release strength, f'ci) indicated in the Contract documents. Do not begin tensioning operations until after the Engineer approved patches or repairs have been satisfactorily completed. Do not tension the prestressing steel until all concrete in the member has been placed.

Perform stressing of tendons in conformance with the sequence shown on the approved shop drawings and to the satisfaction of the Engineer. Stress tendons in such a sequence that lateral eccentricity of prestress and loss of prestress will be a minimum. Stress tendons symmetrically about the center of the typical section so no more than one tendon is eccentric about the centerline at any one time. Sequence the stressing of the tendons so the individual tendon force does not exceed the tendon force in all other tendons by more than 50 percent of the final jacking force of the tendon at any one time.

Stress all strands in each tendon simultaneously. Stress tendons by jacking from only one end of the member unless otherwise approved by the Engineer.

Conduct the tensioning process so that tension being applied and the elongation of the prestressing steel may be measured at all times. Measure elongation to the nearest 1/16 inch. Tension all tendons to a preliminary force between 5 and 25 percent of the final jacking force to eliminate any wedge slip or take-up in the tensioning system before elongation measurements are started. Record the preliminary force so that it can be used in the elongation measurement. Mark at least 25 percent of the strands in each tendon prior to final stressing to permit measurement of elongation and to ensure that all anchor wedges set properly.

For the required tendon force, the observed elongation must agree within 5 percent of the theoretical tendon elongation. In the event the observed elongation is not within acceptable tolerances, determine the source of error and revise the post-tensioning operation to the satisfaction of the Engineer before proceeding. Do not overstress the tendon to achieve the theoretical elongation. No claim for damages or additional compensation or adjustment in Contract time resulting from revisions to the post-tensioning operation will be made or allowed.

Multi-strand post-tensioning tendons having wires that fail, by breaking or slippage during stressing, will be rejected.

Cut post-tensioning steel with an abrasive saw within 1 to 2 inches from the anchoring device. Do not flame cut prestressing steel.

Provide a record of the post-tensioning operation to the Engineer following each tendon installation including, but not limited to, the following:

a.	Project name and bridge number;

b.	Contractor and / or subcontractor name;

c.	Tendon location, size, type;

d.	Date and time tendon was first installed in the duct;

e.	Reel number for strands;

f.	Tendon cross-sectional area;

g.	Modulus of elasticity;

h.	Date and time tendon was stressed;

i.	Jack and gage numbers per end of tendon;

j.	Required jacking force;

k.	Gauge pressure;

l.	Elongation (theoretical and actual);

m.	Anchor set; (anticipated and actual);

n.	Stressing sequence (i.e. tendons stressed before and after);

o.	Stressing mode (one end/ two ends/ simultaneous);

p.	Witnesses to stressing operation (signature); and

q.	Date grouted.

Cover ends of tendons and anchorages immediately after stressing in accordance with Subsection 502-3.02.3.

502-3.03 CAMBER. Camber is the upward deflection that occurs in prestressed concrete flexural members due to the combination of stressing forces and dead load. It does not include dimensional inaccuracies from manufacturing errors.

Form girders so the roadway surface conforms to the indicated grade line with an allowance for 1/2 inch of positive camber at midspan. Form girders to adjust for the predicted long-term camber from loss of prestress and from dead load deflection. When estimating this adjustment, assume that future paving will be applied 3 years after erection.

Control the concrete properties and the placing, curing, curing times, tensioning procedures, and the storage of precast prestressed beam sections. Control these elements so that the shape and amplitude of the deflection curves for all girders will be within specified tolerances and as nearly alike as possible.

Measure camber with the girder supported at bearing points only. When it is impractical to support the girder on its bearing points, you may use alternative support points. Obtain approval of the alternative supports and submit calculations of the effects of the supports on girder camber. Measure actual camber during prestressing force transfer and compare it with computed values and tolerances.

502-3.04 TOLERANCES. Produce prestressed concrete members conforming to the following dimensional tolerances:

- Camber: Do not vary from approved camber more than ±1/8 inch per 10 feet of length, but not to exceed 1 inch. In addition, the camber of any girder may not differ from that of any other girder by more than 1 inch.

- Position of Strands: ±1/4 inch (±1/2 inch where harped strands exit the member).

- Longitudinal Position of Deflection Point for Harped Strands: ±12 inches.

- Position of Ducts and Anchorages: ±1/4 inch

- Position of Local Zone Reinforcement: Center reinforcement on the duct and start within 1/2 inch of the back of the bearing plate.

- Position of Weld Plates: ±1 inch measured along joint. ±1/8 inch transverse to joint.

502-3.05 BONDING AND GROUTING. Conform to the following:

1.	General. Bond post-tensioned prestressing steel to the concrete by completely filling the entire void space between the duct and the tendon with grout. Grout tendons in accordance with the procedures set forth in the approved grouting operation plan. Grout all empty ducts.

2.	Personnel Qualifications. Carry out all grouting operations by workers trained for and experienced in the tasks required. Perform grouting under the immediate control of the post-tensioning technician as described in Subsection 502-3.02.

3.	Grouting Operation Plan. No less than 30 days prior to the initiation of production grouting, submit a grouting operation plan to the Engineer for approval. Devise the grouting procedures to ensure that the ducts will be properly filled by grout. As a minimum, address and provide procedures for the following items in the grouting operation plan:

a.	Type, quantity, and brand of materials used in the grouting including all material certifications;

b.	Type of equipment furnished, including capacity in relation to demand and working condition, as well as back-up equipment and spare parts;

c.	Types and locations of vents;

d.	Types and sizes of grout hoses and connections;

e.	Theoretical grout volume calculations;

f.	General grouting procedure;

g.	Duct cleaning method prior to grouting;

h.	Mixing and pumping procedures;

i.	Type and frequency of quality control production tests;

j.	Direction of grouting;

k.	Sequence of use of the vents;

l.	Method to be used to control the rate of flow and pressure within the ducts;

m.	Procedures for handling blockages, including flushing of ducts;

n.	Procedures for possible post grouting repair; and

o.	Names of the persons in charge and the other personnel who will perform the grouting operation, including their relevant certification, experience, and skill.

Do not commence production grouting until the Engineer provides written approval of the grouting operation plan.

Before initiation of production grouting, conduct a joint meeting with the grouting technician, subcontractors, grouting crew, and the Engineer to discuss the grouting operation plan, required testing, corrective procedures, and other relevant issues.

4.	Grout Storage. Store all grout materials in a dry enclosure or building that is convenient to the work site. Limit on site storage of grout to a maximum period of one month.

5.	Grout Production Tests. Carry out the minimum number of production grout tests as follows:

a.	Grout Strength Test. Prepare grout cube specimens in accordance with ASTM C 942, “Standard Test Method for Compressive Strength of Grouts for Preplaced-Aggregate Concrete in the Laboratory.” Perform a minimum of one strength test per day during grouting operations. Submit strength test results to the Engineer within 24 hours of test completion.

b.	Fluidity test. Perform the modified version of ASTM C 939 “Standard Tests Method for Flow of Grout for Preplaced-Aggregate Concrete (Flow Cone Method)” Test as specified in Subsection 701-2.05. Repeat testing at least every two hours of grouting operations. Submit fluidity test results to the Engineer within 24 hours of test completion.

6.	Field Trial Test. Demonstrate to the satisfaction of the Engineer that the grouting equipment, methods, and procedures are appropriate. Conduct field trial tests at least seven days prior to initiation of production grouting or as specified by the Engineer. Perform batching and testing with the same materials, personnel, and equipment used in production grouting. Furnish all materials and labor at no cost to the Department.

7.	Preparation of Enclosures. If a corrosion inhibitor, or any other material other than prestressing steel is inside the duct, flush the ducts using a solution of quick lime (calcium oxide) or slaked lime (calcium hydroxide) in the amount of 0.1 lbs/gal.

Blow duct with oil free compressed air to remove water and debris blockages that may interfere with the injection of grout.

Inspect valves to be sure that they can be opened and closed properly. Check that the grout hose connections and inlets are free of dirt.

8.	Equipment. Provide grouting equipment consisting of measuring devices for water, a high-speed shear colloidal mixer, a storage hopper (holding reservoir) and a pump with all the necessary connecting hoses, valves, and pressure gauge. Provide grouting equipment with sufficient capacity to ensure that the post-tensioning ducts to be grouted can be filled and vented without interruption in less than 20 minutes.

Provide an air compressor, flushing equipment, and hoses with sufficient output to perform the required functions.

At the direction of the Engineer, provide vacuum grouting equipment (volumetric measuring type) in the event that voids are encountered after the grouting operation is complete. No additional compensation will be made in the event that vacuum grouting equipment is required.

Provide the following equipment:

a.	Mixing Equipment. Provide a high speed shear colloidal mixer capable of continuous mechanical mixing producing a homogeneous and stable grout free of lumps and un-dispersed cement. Use only colloidal grout machinery that has separate charging and storage tanks. Equip the charging tank with a high shear colloidal mixer and fit the storage tank with an agitator to keep the grout moving continuously before it is pumped into the duct. Use grouting equipment with a gravity feed to the pump inlet from the storage tank.

Include a screen having clear openings of 1/8 inch maximum size to screen the grout prior to its introduction into the grout pump or storage hopper. Locate the screen between the charging tank and the storage tank so that the screen is easily accessible for inspection and cleaning.

Keep the holding tank agitated and at least 1/4 full at all times during the pumping operation to prevent air from being drawn into the post-tensioning duct.

Periodically inspect the screen during grouting operations. Do not use grout if lumps of cement remain on the screen.

Add water during the initial mixing by use of a calibrated flow meter or calibrated water reservoir with a measuring accuracy equal to one percent of the total water volume. Where water is not supplied through the public water supply system, provide a water storage tank of sufficient capacity.

b.	Grout Injecting Equipment. Provide pumping equipment capable of continuous operation with little variation of pressure that includes a system for circulating the grout when actual grouting is not in progress.

Use positive displacement type grout pumps that provide a continuous flow of grout and will be able to maintain a discharge pressure of at least 145 psi. Use grout pumps with adequate capacity so that an optimal rate of grouting can be achieved. Ensure pumps are constructed to have seals adequate to prevent oil, air or other foreign substances entering the grout and to prevent loss of grout or water.

Use equipment capable of maintaining pressure on completely grouted ducts and fitted with a valve that can be closed off without loss of pressure in the duct.

Install a pressure gauge having a full-scale reading of no more than 290 psi at the duct inlet. If hoses in excess of 100 feet total length are used, place and use two gauges, one at the pump and one at the inlet.

Use grout hoses with sufficient diameter, rated pressure capacity and that are compatible with the pump output. Install a sampling tee with stopcock that minimizes the number of bends, valves, and changes in diameter. Firmly connect grout hoses to pump outlets, pipes, and duct inlets.

Do not use compressed air to aid the pumping of grout.

c.	Air Compression. Provide equipment to supply oil-free and water-free compressed air to blow out excess water and to check the free passage of the ducts.

d.	Flushing Equipment. Provide standby flushing equipment using a potable water supply to facilitate complete removal of grout from the duct if difficult grouting conditions exist. This equipment is in addition to the grouting equipment. Utilize a different power source than the grouting equipment. Furnish equipment that is capable of delivering a pressure of at least 290 psi to flush out partially grouted enclosures.

e.	Vacuum Grouting Equipment. At the direction of the Engineer, provide vacuum grouting equipment. Use volumetric measuring type vacuum grouting equipment with the ability to measure a void and supply a measured volume of grout to fill the void.

f.	Standby Equipment. During grouting operations, provide a standby grout mixer and pump.

9.	Mixing of Grout. Mix grout using the entire contents of each bag in accordance with the manufacturer’s recommendations and using a metered amount of water. Mix the materials thoroughly to produce a homogeneous grout without excessive temperature increase or loss of properties. Do not mix grout longer than the manufacturer’s recommended duration. Continuously agitate the grout until grouting is complete.

Check the fluidity of the grout in accordance with Subsection 701-2.05. Do not commence grout pumping until fluidity requirements are satisfied.

Do not add water to increase fluidity that has decreased by delayed use of the grout.

10.	Injection of Grout. Use a method of injecting grout that will ensure complete filling of the ducts and complete encasement of the prestressing steel.

Open all grout vents before commencing grouting operations, unless otherwise approved by the Engineer.

Perform grouting in one operation, maintaining a continuous, one-way flow of grout at all times within a grouting stage. Grout tendons from the lowest vent in an uphill direction. Unless approved otherwise by the Engineer, pump grout at a rate of 15 feet to 50 feet of duct per minute to avoid air entrapment, segregation of the grout, and to ensure complete filling of the duct. Conduct normal grouting operations at a pressure range of 10 psi to 75 psi measured at the grout inlet. Do not exceed the maximum pumping pressure of 145 psi at the grout inlet.

Pump grout through the duct and continuously discharge grout from the first and subsequent outlets until any residual water and entrapped air has been removed and the consistency of the grout is equivalent to that of the grout being pumped into the inlet. Discharge at least 1/2 gallons of grout from each outlet prior to closing the vent. Close all outlet vents in a similar manner one after another in the direction of flow except that at intermediate crests, close outlet vents placed a short distance downstream of the crest before closing their associated high point vent. Discarded grout does not represent additional cost to the Department.

Pump grout through the duct and continuously discharge grout, to the satisfaction of the Engineer, at the anchorage and grout cap outlets until all free water and air are discharged and the consistency of the grout is equivalent to that of the grout being pumped into the inlet. Close the anchorage outlet vent and discharge a minimum of 1/2 gallon of grout from the grout cap. Close the grout cap outlet.

After all outlets have been bled and sealed, bleed the grout pressure to 5 psi and wait a minimum of ten minutes for entrapped air to flow to the high points. After ten minutes, increase the pressure as needed and discharge grout at each high point outlet to eliminate all entrapped air or water. Complete the process by locking a pressure of 30 psi into the tendon prior to closing the inlet vent.

If the actual grouting pressure exceeds the maximum allowed, close the inlet vent and pump grout at the next outlet, which has just been or is ready to be closed, as long as one-way flow is maintained. Do not pump grout into a succeeding outlet vent from which grout has not yet flowed. If this procedure is used, equip the new inlet vent with a positive shut-off and pressure gage.

11.	Temperature Considerations. Do not grout if the ambient air temperature exceeds 100°F. Do not grout if the ambient air temperature is expected to be less than 40°F within 48 hours. Ensure grout temperature upon mixing is between 50°F and 90°F.

If the ambient air temperature is below 32°F, keep ducts free of water to avoid damage due to freezing. Do not warm ducts with steam. Blow dry air (60% humidity or less) through the ducts to extract trapped water. Ensure ducts are free of frost and ice before commencing grouting operations.

12.	Post-Grouting Inspection. Do not remove or open vents until the grout has cured for at least 24 hours. After the grout has cured, remove all outlets and grout caps located at anchorages and high points along the tendon to facilitate inspection. If voids are suspected or if duct grouting operations were prematurely terminated prior to completely filling the duct, explore the voided area inside the duct with an endoscope, borescope, videoscope, or other visual means approved by the Engineer. Probing is not allowed. Determine the location and extent of all voided areas.

Depending on the location of the void, drilling may be required to penetrate the inner surface of the anchorage or duct. Use drilling equipment that will automatically shut-off when steel is encountered.

13.	Repairing and Filling Voids. Repair and fill all voids that occur in the ducts after the grouting operation is complete. If voids are found, submit a grouting repair plan to the Engineer for review and approval that describes the location and extent of the void and the method of repairing and filling the void. If the extent and location of the void is such that complete filling of the void is not possible using the grout injection equipment, repair and fill the void using a volumetric measuring vacuum grouting process utilizing the vacuum grouting equipment specified in Subsection 502-3.05.8.

14.	Finishing. Remove all valves, caps and pipes for each vent to a depth at least 1 inch below the surface of the concrete. Fill the void left by the vent pipe according to Subsection 501-3.10.1. Do not remove or open vents until the grout as set for at least 24 hours.

15.	Protection of End Anchorages. Within seven days upon completion of the grouting, permanently protect the anchorage of post-tensioning tendons to prevent access of water or other aggressive agents.

Immediately before casting the concrete pour-backs (within 24 hours.), mechanically clean and roughen the mating concrete surfaces to remove any laitance and to expose small aggregate. Use abrasive blast cleaning or water blasting with a pressure washer capable of at least 10,000 psi nozzle pressure at all elevations to clean the concrete surfaces. Keep the nozzle tip no more than 12 inches from the surface during all phases of water blasting. Flush the surface with water and blow dry. Ensure surfaces are clean, sound and without standing water.

Unless otherwise specified in the Contract documents or shown on the approved shop drawings, ensure the prestressing steel and all parts of the anchoring assemblies are at least 3 inches inside of the end surface of the member. Apply an epoxy bonding agent to the concrete mating surfaces according the manufacturer's instructions. Fill the recess with concrete and finish the concrete surface to true lines according to the Contract requirements.

16. 	Record of Grouting Operation. Submit a written report to the Engineer within 72 hours after grouting. Include in this report:

a.	the date of grouting;

b.	the number of days from tensioning to grouting;

c.	the tendons grouted;

d.	the quantities and types of materials used;

e.	the volume of grout pumped into the duct

f.	a summary of problems encountered during grouting and steps taken to resolve them;

g.	the maximum pumping pressure at the inlet;

h.	the temperature measurement of the air, water, prepackaged material, mix grout, and concrete member in the duct.

i.	the results of quality control testing.

502-4.01 METHOD OF MEASUREMENT. Section 109.

502-5.01 BASIS OF PAYMENT. The lump sum payment is full compensation for furnishing, installing, stressing, grouting, repairing, and inspecting all post-tensioned tendons accepted in place.

All items of the post-tensioning system embedded within the concrete including but not limited to prestressing steel, enclosures for prestressing steel, wedges, wedge plates, anchorage assemblies and associated supplemental reinforcing steel required by the supplier, grout vents, and grout gaps are subsidiary to post-tensioned concrete structural members.

All post-tensioning system hardware that is not embedded in concrete including but not limited to jacks, gauges, wire socks, and torpedoes are subsidiary to post-tensioned concrete structural members.

All items and equipment to fill the ducts with grout including but not limited to mixers, gauges, flushing equipment, and production tests are subsidiary to post-tensioned concrete structural members.

All materials for protecting the post-tensioning steel and anchorages including but not limited to corrosion inhibitors, flushing equipment, concrete bonding agents, and equipment to prepare the concrete block-outs are subsidiary to post-tensioned concrete structural members.

All labor, materials, tools, equipment and incidentals necessary for completing the work are subsidiary to post-tensioned concrete structural members.

Payment for prestressing precast concrete members is included in the Contract price paid for the precast members, as provided for Section 501.

52035-022511