SECTION 513

FIELD PAINTING OF STEEL STRUCTURES

Susitna Bridge Repairs: refer to Section 202 Removal of Structures and Obstructions, 501 Structural Concrete, 504 Steel Structures, 507 Bridge Railing, 512 Forms and Falsework, 514 Bearing Replacement, 515 Polyester Concrete Overlay, 720 Friction Pendulum Bearings and 731 Polyester Concrete for further repairs or see archived project specifications 58247.

Special Provision

513-1.01 DESCRIPTION.  Add the following:

Except for the stay-in-place metal forms, clean and paint all exposed superstructure steel including, but not limited to the main girders, stringers, floor trusses, lateral bracing and miscellaneous stiffeners and connection plates.  The existing paint system on the Susitna River Bridge consists of a Red Lead, Iron Oxide and Linseed Oil prime coat and intermediate coat conforming to SSPC Specification Paint 14 and an Aluminum paint top coat.

Clean and paint existing steel faying surfaces prior to installing new steel members.

513-3.09 Containment and disposal.  Add the following:  The presence of lead is expected in the existing paint system.

513-3.10 Surface Preparation.  Add the following to the fourth paragraph:  Add CHLOR*RID (liquid soluble salt remover) or approved equal to the pressure washer feed water.

513-3.12 Painting Metal Surfaces.  Insert the following after the ninth paragraph:  Apply only a mist coat (0.5 to 0.8 mil dry film thickness) of inorganic zinc-rich primer, meeting SSPC Paint Specification No. 30, Weld-Through Inorganic Zinc Primer, Class 5, on the following surfaces:

- High strength bolted connection contact surfaces.  Use primer that is qualified by test as a Class B coating according to the document “Test Method to Determine the Slip Coefficient for Coatings Used in Bolted Joints” as adopted by the Research Council on Structural Connections.

- Areas within 2 inches from edges to be welded

- Areas where the full 3 coats of paint will interfere with field assembly

(9/13/06)BRIDGE