- SECTION 610

DITCH LINING

Special Provisions

610-2.01. MATERIALS.  Add the following:

Use well graded stones that are hard, angular, and have no more than 50% wear at 500 revolutions as determined by AASHTO T 96.  Use stones with breadth and thickness at least 1/4 of its length.  Do not use rounded stones.

55260/56176-040914