- SECTION 611

RIPRAP

Special Provisions

611-2.01 MATERIALS.  Add the following after the first sentence:

Apparent specific gravity will be determined by WAQTC FOP for AASHTO T85.

CR277-110705

Add the following after Item 4:

5.	Class 1A		0-10% weighing less than 3 pounds

60-80% weighing less than 25 pounds

95-100% weighing less than 40 pounds

611-3.01 CONSTRUCTION REQUIREMENTS. Replace the third paragraph with the following:

Place the stones on prepared slopes within the limits shown on the Plans or as directed by the Engineer. Construct a uniform and regular surface with slopes no steeper than those shown on the Plans. Maintain the riprap until final acceptance, and replace any displaced material to the design slopes, lines, and grades at the contractor’s expense.

Place materials in a manner that produces a well-keyed mass of stone. Stones in Class III and Class IV lifts shall be placed with each individual stone having at least three points of contact. Ensure that finished surfaces of all layers are free from pockets of single sized stone. Placement of small stone to choke the spaces between large stones or for leveling the surface is not permitted. Breaking of individual pieces in place by blasting or mechanical methods is not permitted. Place filter or underlayer stone to the full course thickness at one operation and in a manner that avoids displacing underlying materials. Placement by methods likely to cause segregation, such as end dumping, side dumping or pushing into position with earth-moving equipment, are not permitted. Obtain the desired distribution of various sizes of stones throughout the mass by selective loading and by controlled placement of successive loads during placement. Materials that do not meet the specified requirements for size, quality or distribution of sizes will not be allowed for use.

Add the following subsection:

611-3.02 SALVAGE AND REPLACE EXISTING RIPRAP.

Areas exist where existing Class III to Class IV riprap must be moved to facilitate embankment repairs. Existing stones shall be stockpiled for reinstallation after embankment repairs have been made. Stockpiles may be on-site, but cannot be located below the ordinary high water line. Rounded rock, generally less than 25 pounds each, has been used for temporary embankment repairs. This rock shall be salvaged and delivered to the Homer Maintenance Station.

After embankment repairs have been made according to the Plans, replace the stockpiled Class III and Class IV riprap in accordance with the Plans and Subsection 611-3.01. Existing subgrade material excavated to key in the replaced riprap shall be embanked at the toe of the riprap slope.

611-5.01 BASIS OF PAYMENT. Add the following:

Salvage and Replace Existing Riprap consists of salvaging existing riprap, stockpiling and resetting stones meeting class III and class IV specifications, and delivering smaller stone material to the Homer Maintenance Station. Keying replaced stones into the existing slope is subsidiary.

Add the following Pay Items:

Pay Item No.	Pay Item	Pay Unit

611(1A)	Rip Rap, Class 1A	Cubic Yard

611(1B)	Rip Rap, Class IV	Cubic Yard

611(3)	Salvage and Replace Existing Riprap	Station

55260-040914