- SECTION 619

SOIL STABILIZATION

Special Provision

619-1.01 DESCRIPTION. Add the following:

This work also consists of furnishing, placing and maintaining Cellular Slope Protection where shown on the Plans or as directed by the Engineer.

619-1.02 SUBMITTALS. Add the following:

Submit a Manufacturer’s Certificate of compliance as defined in Subsection 106-1.05, Certification of Compliance, for all materials to be placed under Item 619(6) Cellular Slope Protection.  Include the manufacturer’s installation instructions for the application shown on the Plans.

619-2.01 MATERIALS. Add the following:

1.	General. Use cellular slope protection systems pre-manufactured as an assembly of expandable connected cells constructed of high-density polyethylene (HDPE).  Use non-perforated cell walls.  Firmly anchor the slope protection as recommended by the manufacturer.

2.	Cellular Slope Protection System. Use one of the following cellular slope protection systems or an approved equivalent:

a.	“Geoweb 4” Standard Cell”, as manufactured by Presto Products Company, P.O. Box 2399 Appleton, Wisconsin, 54913, (800) 548-3424

b.	“EnviroGrid 4”, as manufactured by AGH Industries, Inc., P.O. Box 1852, Fort Worth, Texas, 76101, (817) 284-1742

c.	“GeoLok 400”, as manufactured by Fluid Systems, Inc., 1245 Corporate Boulevard, Suite 300, Aurora, Illinois, 60504, (800) 346-9107

3.	Prefabricated Slope Protection System Material: Shall meet the following requirements:

Nominal Cell Depth (min.)	4 inches

Sheet Thickness (min.)	50 mil ± 5 mil

Tensile Seam Strength (min.)	225 lbf

Standard Sheet Configuration (typ.)	8 feet x 20 feet

Individual Expanded Cell (max.)	10 inches x 8 inches

Add the following Subsection:

619-3.04 CELLULAR SLOPE PROTECTION. Construct the cellular slope protection according to the details on the approved working drawings and consistent with the manufacturer’s recommendations.

Foundation Preparation. Construct slopes to the lines and grades shown on the Plans prior to construction of the cellular slope protection.  Level or fill localized high or low spots.  Remove all obstructions such as projecting stones.  Remove soft or low-density pockets of material and backfill with selected material.

Construction Requirements. Place the cellular slope protection mats in such a manner as to produce a smooth surface and construct within the specified lines and grades shown on the Plans.  Follow the manufacturer’s recommendations for construction of the cellular slope protection system.

Stretch the mat to the standard nominal expanded dimensions and anchor it according to the manufacturer’s recommendations.  Place the mats side by side so that the mats interlock.  Join or anchor the mats according to the manufacturer’s recommendations.

Infill the cells with topsoil to a depth of 2 inches above the cell walls.  Compact the topsoil with a smooth excavator bucket or with hand equipment.

619-4.01 METHOD OF MEASUREMENT. Add the following:

Item 619(6) Cellular Slope Protection shall be measured by the square yard on the slope of the ground surface.  Payment for seeding Cellular Slope Protection topsoil infill shall be paid for under Item 618(1A) Seeding, Type A.  Payment for infilling Cellular Slope Protection with topsoil shall be paid for under Item 620(1B) Topsoil, Class B.

There will be no separate measurement for hardware and geotextile necessary for Cellular Slope Protection as it will be considered subsidiary to Item 619 (6).

619-5.01 BASIS OF PAYMENT.

Add the following Pay Item:

| Pay Item | Pay Unit |
| --- | --- |
| 619(6) Cellular Slope Protection | Square Yard |