SECTION 635

INSULATION BOARD

Special Provisions

635-1.01 DESCRIPTION. Add the following: Insulation will be placed between a storm drain and a sanitary sewer or waterline when the separation is less than 3-feet. This work will also consist of placing a sand blanket bedding under and over the horizontal insulation boards.

635-2.01 MATERIALS. Delete this subsection in its entirety and add the following: Use materials that conform to the following:

Insulation Boards. AASHTO M 230 96, Type VII, except that extrusion is not required and the maximum water absorption by weight is 10%, as determined by ASTM C 272.  Meet or exceed the minimum R Value listed in the insulation board table below.

Insulation Board Table

Thickness Per Plan	Minimum Compressive Strength	Minimum R-Value

1 inch	60 psi	5.0

2 inch	60 psi	10.0

3 inch	60 psi	15.0

Sand Blanket.  Subsection 703-2.12.

635-3.01 CONSTRUCTION REQUIREMENTS. Delete the second paragraph and substitute the following: The horizontal insulation board shall be laid on a sand blanket leveling course, and covered with sand blanket material, spread and compacted to a depth of 4-inches prior to the placing of subsequent lifts.  Spreading and compacting equipment shall be approved by the Engineer.

635-4.01 METHOD OF MEASUREMENT. Delete this subsection in its entirety and replace with the following: By the horizontal square yard of insulation board, in place, complete and accepted. Sand blanket material will not be measured for payment.

635-5.01 BASIS OF PAYMENT. Add the following: Sand blanket material will not be paid for separately, but will be subsidiary to Item 635(1) Insulation Board.

Under Pay Unit, delete MBM and replace with the following: Square Yard.