SECTION 702

ASPHALT MATERIALS

Special Provision

- Add the following Subsection:

702-2.05  SAND SEAL ASPHALT.  GSB 78 or meet the following:

Kinematic Viscosity at 140 degrees Fahrenheit (60C), AASHTO T 201, cts...................... 	10-30

Percent Water, AASHTO T 55, Maximum..........................................................................  	0.5

Percent Residue by Distillation, AASHTO T 78, or Evaporation....................................... 	30-45

The residue from distillation shall have the following properties:

Penetration at 25°C (77°F), AASHTO T 49, dmm..............................................................  	2-12

Softening Point, AASHTO T 53, of.....................................................................................  	180-200

Solubility in 1,1,1 Trichloroethylene, AASHTO T 44, %......................................................  	99 min.

HCL Precipitation Value................................................................................................ 		18-25

The bituminous base residue shall contain not less than 35 percent gilsonite, and shall not contain any tall oil pitch.  Curing time, under recommended application conditions, shall not exceed 4 hours.  The Contractor shall furnish and submit to the Engineer, manufacturer’s certification that the material is the type, grade, and quality specified for each load of bituminous material delivered.  The certification shall show the shipment number, refinery, consignee, destination, contract number, and date of shipment.  The contractor shall submit to the Engineer, two 1-quart samples of ready-to-apply bituminous material for each load delivered.