SECTION 703

AGGREGATES

Special Provisions

Add the following subsections:

703-2.13 DRAIN ROCK.  Stone and gravel, uniformly graded from 4 to 8 inches in least dimension and having no more than 60% wear (AASHTO T 96).

703-2.14 FLOWABLE FILL SAND.  Sand containing no muck, frozen material, roots, sod or other deleterious matter and with a plasticity index not greater than 6 as tested by WAQTC FOPs for AASHTO T 89 and T 90.  Meet the following gradation as tested by WAQTC FOP for AASHTO T 27/T 11:

Sieve					Percent Passing by Weight

No. 4					100%

No. 200					0-6%