- Section 705

- Joint Materials

Special Provisions

705-2.02 Joint Sealer.  Delete this subsection and substitute the following:

Backer Rod Material.  Provide extruded backer rod that is soft type, low-density polyethylene, with a skin-like outer texture that will not bond to the silicone sealant.

Joint Sealant.  Use a rapid cure, 100 percent silicone, self-leveling, two-part formulation, and cold applied joint sealant.  Acid cure sealants are not acceptable.  Use a silicone sealant compatible with the surface to which it is applied.  Meet the requirements shown in Table 1 of this specification.

Table 1

Rapid Cure, Silicone Joint Sealant

Part A as supplied:

| TEST | LIMIT | TEST METHOD |
| --- | --- | --- |
| Flow | Self Leveling | ASTM C 639 Type I |
| Extrusion Rate (grams/minute) | 200-550 | MIL-S-8802 |
| Specific Gravity | 1.25-1.34 | ASTM D 972 Method A |

Part B as supplied:

| TEST | LIMIT | TEST METHOD |
| --- | --- | --- |
| Flow | Self Leveling | ASTM C 639 Type I |
| Extrusion Rate (grams/minute) | 180-550 | MIL-S-8802 |
| Specific Gravity | 1.25-1.34 | ASTM D 972 Method A |

As installed at 77F and 50% relative humidity

| TEST | LIMIT | TEST METHOD |
| --- | --- | --- |
| Nonvolatile Content (%, minimum) | 93 | ASTM D 2822 |
| Skin-over Time (minutes, maximum) | 20 | MIL-S-8802 |
| Elongation (1) (%, minimum) | 600 | ASTM D 3583 (2) (3) |
| Modulus (PSI, @100% elongation) | 3-12 | ASTM D 3583 (2) (3) |

(1) Cured 72 hours at 77+- Degrees Fahrenheit and 505% relative humidity.

(2) Section 14 modified

(3) Joint size = ½” x ½” x 2”

Polymer Concrete. Use a two-component rapid-curing liquid polymer that cures to a dense, semi-flexible polymer that is resistant to chemicals, weather, abrasion, and impact and a compatible aggregate.

Meet the requirements as shown in Table 2 of this specification for the binder.

Meet the requirements as shown in Table 3 of this specification for the polymer-based mortar

Table 2

POLYMER NOSING SYSTEM – BINDER

As supplied:  Combined liquid components (base and reactor, 1:1 Ratio by volume)

| TEST | LIMIT | TEST METHOD |
| --- | --- | --- |
| Color | Black | -- |
| Gel Time (minutes) | 20-60 | AASHTO M200 |

As cured: Combined liquid components (base and reactor, 1:1 Ratio by volume)

| TEST | LIMIT | TEST METHOD |
| --- | --- | --- |
| Elongation at Break (%, minimum) | 45 | ASTM D 638 (1) |
| Tensile Strength (PSI, minimum) | 900 | ASTM D 638 (1) |
| Shore D Hardness | 45-75 | ASTM D 2240 |

(1) Molded specimens, .25M Thickness

Table 3

POLYMER NOSING SYSTEM - MORTAR

As cured mortar: Combined liquid components with aggregate

| TEST | LIMIT | TEST METHOD |
| --- | --- | --- |
| Compressive Strength at 24 hours (PSI, minimum) | 2500 | ASTM C 579 (1) |
| Bond Shear Strength (PSI, minimum) | 700 | ASTM C 882 (2) |
| Abrasion Resistance (maximum) | 1.0 | ASTM C 501 Taber H22 |
| Resilience (%, minimum) | 70 | OKLA Test Procedure OHD L6 |

(1) Method B

(2) Or concrete failure