SECTION 709

REINFORCING STEEL & WIRE ROPE

Special Provision

709–2.01  REINFORCING STEEL.  Add the following:

Steel Welded Wire Fabric, Galvanized, for Boardwalk Railing:

- 8GA Welded Wire (0.1644-inch diameter, W2.1xW2.1)

- Wire Spacing Size: 2-inches by 2-inches.

- Galvanized after welding.

- Dimension and Mechanical Properties: ASTM A82 and A496

Staples for Welded Wire Fabric: All staples shall be of9 gauge class 3 galvanized steel or heavier with a minimum length of 2-inches.  Staples shall be barbed and include cutting points.

709-2.02 WIRE ROPE OR WIRE CABLE.  Delete this Section in its entirety and replace it with the following:

Wire rope shall be ¼-inch diameter galvanized aircraft cable in accordance with the following:

- Performance Standard and Dimensions:  Federal Specification MIL-DTL-83420M

- Material:  Drawn galvanized high carbon steel per Federal Specification MIL-DTL-83420M

- Working Load Limit:  1,400 lbs.

- Minimum Breaking Strength:  7,000 lbs.

Wire rope clips shall be ¼-inch  malleable steel in accordance with the following:

- Material and Mechanical Properties:  Federal Specification FF-C-450D Type I Class 2.

- Saddle Hardness:  HRB 83 maximum.

- Thread Requirements:  Nut Fit, Threads are acceptable when torque tested per FF-C-450D

- Coating:

  - U-Bolt and Nuts:  Fe/Zn3A per ASTM F1941.

  - Saddle: Hot dipped galvanized per ASTM A153 or F2329.