- SECTION 712

MISCELLANEOUS

Special Provisions

712-2.17 METHYL METHACRYLATE PAVEMENT MARKINGS.  Replace No. 1. Quality Requirements: with the following:

1.	Quality Requirements:  Use a marking material formulated for the application type specified.  Use a marking material manufactured from new materials and free from dirt and other foreign material.  Use a methyl methacrylate based resin system for part “A”.  Use benzoyl peroxide system for part “B”.

Extruded or stenciled application:  Material formulated for extruded or direct stenciled application with factory intermix beads, and anti skid aggregate and the application of additional surface applied beads.

Submit a manufacturer certification for both the methyl methacrylate material, glass beads and anti-skid aggregate to ensure that the materials furnished conform to these Specifications.

2.	Performance Properties:  Add the following:

I.	Color:	Yellow, PR-1 Chart, 33538 Federal Yellow.  White, minimum daylight reflectance of 84.

712-2.18 GLASS BEADS FOR METHYL METHACRYLATE PAVEMENT MARKINGS.  Replace the bead table with the following:

Use the type and quantity of beads specified in writing by the marking material manufacturer required to satisfy the specified performance requirements.  The written certification will note the bead coating is compatible with the marking material binder.

1.	Bead Manufacturer and Type.

a.	Swarco, Megalux-Beads or

b.	Approved equal beads

Approved Equal Beads.  Equal beads will demonstrate:

(1)	Bead coatings compatible with marking materials.  Marking Material Manufacturer will certify compatibility.

(2)	Lasting retro reflectivity.

CR246-010109

Add the following:

712-2.19 EPOXY CARTRIDGE SYSTEM.  Use an epoxy cartridge system that consists of the following:

1.	A bonding material that is a two-component epoxy contained in a cartridge having two separate chambers

2.	An applicator that is a special dispensing gun having a replaceable static mixing nozzle.

3.	Use an epoxy cartridge system appropriate for the service temperature and ambient concrete temperature at the time of installation.

Epoxy cartridge systems are subject to the approval of the Engineer. Use epoxy cartridge systems that meet the requirements of the “Acceptance Criteria for Adhesive Anchors in Concrete and Masonry Elements,” AC58, by the International Code Council Evaluation Service (ICC-ES). Meet the suitability requirements for creep, in-service temperature, dampness, freezing and thawing, and seismic qualification of these acceptance criteria. Approval of epoxy cartridge systems is contingent upon the Contractor submitting to the Engineer one sample of each type of epoxy cartridge system, manufacturer’s installation instructions, and certified results of tests, either by a private testing laboratory or the manufacturer, indicating compliance with the above requirements.

Unless shown otherwise, do not use epoxy cartridge systems when:

1.	Temperature of concrete is above 110°F or below 40°F

2.	There is a likelihood of fire

3.	Coated bars or rods are specified unless the embedment depth is increased by 50%

Provide epoxy cartridges clearly and permanently marked with the manufacturer’s name, model number of epoxy cartridge system, manufacturing date, and lot number. For each carton of epoxy cartridges, provide the manufacturer’s recommended installation procedures, minimum cure time, and such warning or precautions concerning the contents as may be required by State or Federal Laws and Regulations.

Provide a certificate of compliance with each shipment of the epoxy cartridge system, regardless of which epoxy product is furnished, as provided in Section 106-1.05. Provide a certificate of compliance to the Engineer that the repair procedure using the epoxy cartridge system was completed in conformance with the manufacture's recommendations.

712-2.20  EPOXY RESIN MORTAR.

Use epoxy resin binder meeting AASHTO M235, Type I, Grade 3 (Non-sag).  Develop a 28 day compressive strength of 5000 psi.

712-2.21  EPOXY RESIN ADHESIVE.

Use epoxy resin adhesive meeting AASHTO M235, Type I, Grade 3 (Non-sag).

52081-050212